# ASSESSING PIEZO FILM SENSORS FOR MINING APPLICATIONS

Author: Zhassulan Karimzhan
(16zk4@queensu.ca)

Supervisors: Prof. Laeeque Daneshmend and Prof. Oscar Rielo

The Robert M. Buchan Department of Mining
Queen’s University

Mine – 434 Project Report

Submission Date:

# ASSESSING PIEZO FILM SENSORS FOR MINING APPLICATIONS

# ABSTRACT

The purpose of the project is to conduct a study on piezo-film sensors from the company “TE Connectivity” to determine its characteristics in transient and vibrational environments. The results were compared to the characteristics of traditional strain gauges. The goal of the project is to identify the more viable sensor in the mining industry. Results show that piezo-film sensors outperform strain gauges in transient and vibrational environments. Advantages of piezo-film sensors are that they do not need an input source of power, produce less noise, resilient and cheap. It is recommended to perform more testing with applications in engines, mills, impact monitoring and VOD analysis to confirm the reliability of results.

KEYWORDS

Strain Gauge, Piezo film, Sensor, Accelerometer, Transient, Vibration, Fast Fourier Transform (FFT), Split Hopkinson pressure bar, Sieving table, Linear Regression.

INTRODUCTION

It is proposed that piezo film sensors from the company TE connectivity can perform more than their current utilization, with a focus on mining industry applicability. The goal is to characterize and calibrate the sensors in static, transient and vibrational environments. In the mining industry, several critical activities that follow the characteristics we aspire to calibrate. Dynamic measurements in mining include blasting and micro seismic activities. Vibrational measurements in mining include health and safety monitoring and maintenance and reliability monitoring. The purpose of the experiment is to replace traditional sensors, like strain gauges or accelerometer, with TE connectivity’s sensors within the mining environment. Piezo film sensors prove to be more economical, are passive sensors and can be used repeatedly. Data acquisition system including the voltage divider to condition the sensor input must be set up prior to lab experiments. After the experiments, data will be analyzed to test the linearity of data and the possibility to use the sensors as replacements to previous devices.

## Strain gauge

A strain gauge is a sensor which responds to the expansion or contraction of a material, or the strain. The sensor usually consists of metallic wire (resistor) in a grid pattern which maximizes the amount of strain or deformation of the gauge in a certain direction. The electrical resistance of metallic grid changes in proportion to the amount of strain experienced by the test specimen. The grid is bonded to a thin backing called the carrier. The carrier is bonded directly to the strained surface by a thin layer of adhesive. When a load is applied to the test specimen, the resulting change in length is communicated to the resistor and the corresponding strain is measured in terms of the electrical resistance of the grid, which varies linearly with strain. A voltage is provided to the gauge while it is being used to measure these small changes in resistance which are proportional to the strain within the gauge and therefore the test specimen as well (National Instruments, 2019). Figure 1 shows an example of a strain gauge.

Figure 1. Strain gauge

Application of strain gauges have several necessary conditions and difficulties, which are:

- Strain measurements rarely involve quantities larger than a few millistrain; therefore, very small changes in the signal from the gauge must be accurately measured,

- Setting Wheatstone bridge arrangements to detect small changes in resistance,

- A voltage source to power the circuit,

- Remote sensing to compensate for errors in excitation voltage from long lead wires,

- Amplification to increase measurement resolution and improve signal-to-noise ratio,

- Filtering to remove external, high-frequency noise,

- Offset nulling to balance the bridge to output 0 V when no strain is applied (National Instruments, 2019).

## Piezo film

Piezo film sensors are based on the concept piezoelectric effect, which is the generation of electricity due to mechanical deformation. The sensor is flexible, lightweight, tough engineering plastic available in a variety of different sizes, thicknesses and shapes. In its simplest mode, the film behaves like a dynamic strain gauge except that it requires no external power source. Piezo film transducers may often cover a much larger area than standard strain gauges, so any direct comparisons should be performed in a uniform strain field for meaningful results (Measurement Specilaties, Inc., 1999). The selected piezo films for this study were obtained from “TE Connectivity”. From this company, FDT series piezo film sensors were used which is displayed in Figure 2.

Figure 2. FDT series piezo film sensors

Some general piezoelectric film properties include:

- Wide frequency range—0.001 Hz to 109 Hz,

- Vast dynamic range (10-8 to 106 psi or μ torr to Mbar),

- Low acoustic impedance,

- High elastic compliance,

- High voltage output,

- High dielectric strength withstanding strong fields up to 75 V/μm,

- High mechanical strength and impact resistance (109 to 1010 Pascal modulus),

- High stability: resisting moisture (<0.02% moisture absorption), most chemicals, oxidants, and intense ultraviolet and nuclear radiation.

## Accelerometer

Piezo electric accelerometer is an accelerometer that uses the effect of piezoelectricity to measure dynamic changes in mechanical variables. A seismic mass is connected to the piezoelectric material inside the accelerometer. Due to the piezo electric effect, a charge output proportional to the applied force is generated. As the seismic mass is constant, the charge output signal is proportional to the acceleration of the mass (Metra Mess-und Frequenztechnik, 2001). Dytan’s 3055D2 accelerometer is selected for this experiment. It is cost effective, low noise and single axis accelerometer. Figure 3 shows the accelerometer that is used.

Figure 3. Accelerometer

Some general accelerometer properties include:

- Extremely wide dynamic range, low output noise - suitable for shock measurement as well as for almost imperceptible vibration,

- Excellent linearity over their dynamic range,

- Wide frequency range (1 to 10000 Hz),

- Compact yet highly sensitive (100 mV/g),

- No moving parts - no wear,

- Self-generating - no external power required (Metra Mess-und Frequenztechnik, 2001).

To read the signals from accelerometer, a charge amplifier is being used. Kistler’s 5010B type charge amplifier is selected for this experiment. The charge amplifier converts the charge signal from a high impedance piezoelectric acceleration type sensor into a high level output voltage and provides excitation power along with signal processing for voltage mode type sensors. Figure 4 shows the charge amplifier that was used in this experiment.

Figure 4. Charge amplifier

# EXPERIMENTAL AND RESEARCH METHODOLOGY

## Data acquisition setup

HBM’s QuantumX MX1615B data acquisition system (DAQ) will be used to acquire the data provided by sensors. The data is then be analyzed using MATLAB software. A simple circuit with the piezo film sensor will be created which includes a voltage divider. The voltage divider must be used to reduce the output of the film sensors from their voltage of 10 mV up to 100 V (TE Connectivity, 2019) so that it stays within the 10 V range while performing experiments so the wires will not burn. The voltage divider circuit is shown in Figure 5 where piezo film sensor is represented as Vin, R1 and R2 as resistors where R2 is eight times the R1 (R2=8R1) and Vout is the connection to the DAQ.

Figure 5. Voltage divider circuit involving the Piezo film sensor (represented by Vin) followed by resistors (R1 and R2)

Figure 6 shows the assembled voltage divider circuit that is being used for the experiments. Figure 7 shows the DAQ setup. The sensors must be properly connected to the DAQ (indicated by green light).

Figure 6. Voltage divider circuit

Figure 7. DAQ setup

Figure 8 shows the connectors to the DAQ system. The first connector (on the left) connects strain gauge sensor through channel 2. The strain gauge is configured in quarter bridge circuit and the channel 2 reads signals in µm/m. The second connector (middle) connects Piezo film sensor through channel 3. Reading from PFS were assigned a unit of V (voltage) as there is no engineering unit for this type of readings yet. The third connector (on the right) connects accelerometer through channel 4. Dytran series 3055D2 accelerometer is used for this experiment. Channel 3 reads signals in V.

Figure 8. DAQ connections (Strain Gauge, PFS and Accelerometer respectively)

## Split Hopkinson pressure bar

Split Hopkinson pressure bar (SHPB) is an apparatus for testing the dynamic stress-strain response of materials. Figure 9 shows the schematic of the SHPB technique. A specimen is placed between incident and output bar. A striker bar powered by compressed air hits the incident bar with selected pressure and creates a stress wave propagating through the incident bar, the specimen and the output bars (Wong, 2015). The sensors are mounted to the incident bar and the output bar to record the strains caused by the stress wave pulse.

Figure 9. Schematic of Hopkinson bar

## Transient experiment

The transient characterization of the piezo film sensors will involve the split Hopkinson pressure bar. For the transient test the piezo film sensors will be compared to the strain gauges as a baseline for effectiveness. The piezo film sensor and strain gauge were mounted with adhesive on the incident bar as shown in Figure 10. This experiment did not use any samples, so nothing was placed between incident and output bars. The bars were cleaned prior to any experiments to get rid of the rust to minimize errors. The striking bar must be pushed into the launcher before each test and it is shown on the left in Figure 11. The compressed air and firing valves which cause the release of the striking bar are shown on the right in Figure 11.

Figure 10. Strain gauge and piezo film sensor installed on incident bar

Figure 11. Left: Striking bar setup. Right: Compressed air and firing/release valves

The transient experiment involved tests in three different pressures, 50 psi, 100 psi and 150 psi. Four different tests were conducted with each pressure. This was done to find the linearity of the results. During the 100 psi and 150 psi tests the ear protection was worn for safety reasons as the noise level was above normal. Also, the safety cover was placed on top of the striking bar as shown on the left in Figure 11 in case the bar would strike in other direction.

With a strain gauge and piezo film sensor fitted to the incident bar, they were connected to a DAQ and HBM software was used to analyze the data. The needed pressure is adjusted on the pressure valve and the striking bar is released while the software records the data. The sampling rate was 20 kHz with filter frequency of 10 kHz.

## Vibrational experiment

The vibrational characterization of the piezo film sensors will involve the use of the sieving table. For the vibration test the piezo film sensor will be compared with accelerometer and strain gauge. The piezo film sensor and strain gauge were mounted in the middle of metallic ruler with adhesive. Mounting piezo film sensor on the table would result in error in results because there will be no deformation of the sensor. The accelerometer was glued near the piezo film sensor so it will obtain readings at the same position. The ruler is glued to the sieving table on one side while the other side is pinned as shown in Figure 12.

Figure 12. Vibration experiment setup

The vibration experiment included testing the data at three different amplitudes set by sieving table. The chosen amplitudes were 0.5 mm, 1.0 mm and 1.5 mm. Four different tests were performed with every amplitude. Due to the lack of equipment the sieving table that was used could not vary in frequency. The data was collected at a rate of 20 kHz for 10 seconds for each test.

## Safety considerations

Safety training was completed with a supervisor prior to starting the experiments. Precautions were used to reduce the risk of error and fatal outcome. Safety glasses were used during the experiment tests to secure eyes from any airborne objects. Noise cancelling headsets were also used during tests to reduce the risk of hearing damage. During the spit Hopkinson bar experiment, the safety shields were placed over the ignition bar in case of any projectiles.

# ANALYSIS OF RESULTS

## Transient experiment

The results from split Hopkinson pressure bar obtained from DAQ provided waveform data from the strain gauge and piezo film sensors. An example of the data collected by piezo film sensor is depicted in for the 1st test using 150 psi for the striking bar.

Figure 13. Example PFS waveform data collected in split Hopkinson bar test 1 at 150 psi

The scaling analysis was done to find linearity of the data. The analysis was conducted on peaks only and on all domain.

First, the analysis was conducted on the peaks only.  Eight largest peaks were selected on both strain gauge data and piezo film data and corresponding peaks were graphed on scatter plot. The least squares regression was performed to find scaling factor which is the slope of the line. The linear regression lines were obtained from the data provided by 50 psi test 1, 100 psi test 2 and 150 psi test 3 and shown in Figure 14, Figure 15 and Figure 16 respectively.

Figure 14. Peaks linear regression 50 psi 1

Figure 15. Peaks linear regression 100 psi 2

Figure 16. Peaks linear regression 150 psi 3

Second, the analysis was conducted on the whole domain. The selected data were 50 psi test 2, 100 psi test 3 and 150 psi test 1. The least squares regression lines for the whole domain were obtained from MATLAB and shown in Figure 17, Figure 18 and Figure 19 respectively. From the plots of all domain it can be seen that the signals are very noisy as there are much more data.

Figure 17. Linear regression 50 psi 2

Figure 18. Linear regression 100 psi 3

Figure 19. Linear regression 150 psi 1

Figure 20 shows the linear regression line fitted to the data obtained from 150 psi test 4. It can be observed that there is a high concentration of data in the middle of graph and it is due to the failure of the strain gauge for this test as it was not recording proper measurements.

Figure 20. Linear regression 150 psi 4

The summary of scaling factors is shown in Table 1. The scaling factors obtained from the whole domain data are almost identical and the scaling factors obtained from the eight peaks are close to 58. This defines the linearity of the data. Also, based on the linear regression lines the correlation coefficients were found and shown in Table 1. The correlation coefficients are 0.96 and higher which means that data is almost linear.

Table 1 – Transient scaling factors

| Type |  | Scaling Factor | R2 |
| --- | --- | --- | --- |
| Peaks | 50 psi 1 | 56.389 | 0.984 |
|  | 100 psi 2 | 58.038 | 0.997 |
|  | 150 psi 3 | 58.900 | 0.996 |
| Domain | 50 psi 2 | 57.634 | 0.966 |
|  | 100 psi 3 | 57.643 | 0.961 |
|  | 150 psi 1 | 57.823 | 0.971 |

The peaks data from three different pressures are then combined into one and the linear regression line is fitted into combined data and is shown in Figure 21. The correlation coefficient is found to be 0.99.

Figure 21. Peaks linear regression combined

Figure 22 shows the linear regression line fitted into the combined data from three tests 50 psi 2, 100 psi 3 and 150 psi 1. The correlation coefficient decreases to 0.783 due to the increase of the data.

Figure 22. Combined linear regression on whole domain

Also, the dynamic response of the data was compared. For each signal the FFT was performed. An example of the code used in MATLAB to produce the FFT diagrams is provided in the appendix of this document. Figure 23 shows the produced FFT diagram of piezo film sensor at 50 psi 1. It can be observed that at low frequencies there are a lot of signals and it is due to the lack of lubrication on bars. Figure 24 shows the FFT diagram of stain gauge at 50 psi 1.

Figure 23. FFT of PFS at 50 psi 1

Figure 24. FFT of SG at 50 psi 1

From the FFT diagrams it can be observed that there are three distinctive peaks. The values of the peaks were manually identified and tabulated. The frequencies of the peaks are shown in Table 2 and the amplitudes of the peaks are shown in Table 3.

Table 2 - Peaks frequencies

| Frequency (Hz) |  | Peak 1 |  | Peak 2 |  | Peak 3 |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Pressure (psi) | Test # | SG | PFS | SG | PFS | SG | PFS |
| 50 psi | 1 | 1514 | 1514 | 1958 | 2273 | 3027 | 3027 |
|  | 2 | 1514 | 1514 | 1958 | 2290 | 3027 | 3027 |
|  | 3 | 1514 | 1514 | 1956 | 2288 | 3027 | 3027 |
|  | 4 | 1514 | 1514 | 1958 | 2290 | 3027 | 3027 |
| 100 psi | 1 | 1514 | 1514 | 2607 | 2285 | 3027 | 3027 |
|  | 2 | 1509 | 1509 | 1968 | 2275 | 3022 | 3022 |
|  | 3 | 1514 | 1514 | 1963 | 2271 | 3018 | 3022 |
|  | 4 | 1509 | 1509 | 1958 | 2310 | 3018 | 3022 |
| 150 psi | 1 | 1504 | 1504 | 1953 | 2266 | 3018 | 3018 |
|  | 2 | 1514 | 1514 | 1958 | 2275 | 3027 | 3027 |
|  | 3 | 1514 | 1514 | 1958 | 2275 | 3027 | 3027 |
|  | 4 | 1494 | 1494 | 1973 | 2285 | 3027 | 3027 |

Table 3 – Peaks amplitude

| Amplitude |  | Peak 1 |  | Peak 2 |  | Peak 3 |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Pressure (psi) | Test # | SG | PFS | SG | PFS | SG | PFS |
| 50 psi | 1 | 72.4 | 1.1 | 2.8 | 0.0 | 11.9 | 0.1 |
|  | 2 | 92.1 | 1.6 | 1.9 | 0.1 | 17.3 | 0.2 |
|  | 3 | 64.6 | 1.1 | 2.4 | 0.0 | 11.7 | 0.1 |
|  | 4 | 122.0 | 2.1 | 4.3 | 0.0 | 21.8 | 0.2 |
| 100 psi | 1 | 84.8 | 1.5 | 3.8 | 0.1 | 16.6 | 0.2 |
|  | 2 | 124.2 | 2.1 | 6.9 | 0.0 | 23.2 | 0.3 |
|  | 3 | 102.2 | 1.8 | 7.5 | 0.1 | 20.6 | 0.2 |
|  | 4 | 120.5 | 2.1 | 4.7 | 0.0 | 20.4 | 0.2 |
| 150 psi | 1 | 135.2 | 2.3 | 7.1 | 0.1 | 26.7 | 0.3 |
|  | 2 | 52.9 | 0.9 | 11.7 | 0.1 | 10.1 | 0.1 |
|  | 3 | 97.1 | 1.7 | 7.4 | 0.0 | 17.1 | 0.2 |
|  | 4 | 52.9 | 0.9 | 7.9 | 0.0 | 12.8 | 0.1 |

The least squares linear regression line was fitted on data for each peak. Figure 25 shows frequency linear regression on peak 1. It can be observed that frequency of the first peak is identical between piezo film sensor and strain gauge throughout all the data.

Figure 25. Peak 1 frequency linear regression

Figure 26 shows the frequency linear regression of the second peak. It is observed that second peaks are not repeatable and were found at different frequencies. The correlation coefficient was found to be 0.6%.

Figure 26. Peak 2 frequency linear regression

Figure 27 shows the frequency linear regression of the third peak. The third peaks are more linear and repeatable than second peaks with correlation coefficient of 88%; however, they are not identical as the first peak.

Figure 27. Peak 3 frequency linear regression

Figure 28 shows the amplitude linear regression of the first peak. The correlation coefficient was found to be 99.4%. It can be denoted that the amplitude level at first peak is repeatable between tests.

Figure 28. Peak 1 amplitude linear regression

Figure 29 shows the amplitude linear regression of peak 2. The correlation coefficient at this peak is 26.3% which means that at second peak the amplitudes vary in a wider range.

Figure 29. Peak 2 amplitude linear regression

Figure 30 shows the amplitude linear regression at peak 3. The correlation coefficient at this peak was found to be 99.8% and the data is very repeatable and linear.

Figure 30. Peak 3 amplitude linear regression

## Vibrational experiment

Due to settling time of ruler in the vibration experiment two to three seconds of signal was chosen in the middle of each data to do further analysis.

Using the signal analyzer app in MATLAB and using the panner tool ten cycles were chosen for each test and an example is shown in Figure 31. The purple line is the time domain while the orange line is the PFS readings. Using the readings on the data cursors and Equation 2 the average time of the cycle was calculated.

Figure 31. Example of chosen 10 cycles

The frequency of sieving table was calculated using the Equation 1 and it resulted to be around 75 Hz.

f=1Tavg

Equation 1. Sieving table frequency calculation

Tavg=(Tend-Tstart)#cycles

Equation 2. Cycle average time calculation

The amplitude readings for accelerometer are in volts and it should be calibrated into g’s. The calibration certificate was used to make the conversion and is shown in appendix. The interpolation for the sensitivity is done to find the sensitivity value at 75 Hz frequency. A sensitivity value was found to be 100.86 mV/G and is shown in Equation 3.

y=y1+x-x1*y2-y1x2-x1=101.13+75-50*100.59-101.13100-50=100.86

Equation 3. Interpolation of sensitivity

The g values were found using the formula shown in Equation 4.

G=MeasurementSensitivity

Equation 4. G value formula

The calculated frequencies and amplitudes of the vibration data was then tabulated in Table 4.

Table 4 – Calculated frequencies and amplitudes

| Displacement (mm) |  | Frequency |  |  | Amplitude |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | SG | ACC | PFS | SG | ACC | PFS |
| 0.5 | 1 | 76.920 | 76.920 | 76.920 | 226.850 | 1.037 | 3.250 |
|  | 2 | 78.740 | 78.740 | 78.740 | 236.796 | 1.071 | 3.360 |
|  | 3 | 78.125 | 78.125 | 78.125 | 237.028 | 1.130 | 3.381 |
|  | 4 | 78.003 | 78.003 | 78.003 | 238.388 | 1.126 | 3.399 |
| 1 | 1 | 75.131 | 75.131 | 75.131 | 243.275 | 1.022 | 3.241 |
|  | 2 | 75.245 | 75.245 | 75.245 | 246.740 | 1.027 | 3.260 |
|  | 3 | 75.529 | 75.529 | 75.529 | 240.500 | 1.013 | 3.190 |
|  | 4 | 75.472 | 75.472 | 75.472 | 252.200 | 1.091 | 3.378 |
| 1.5 | 1 | 74.129 | 74.129 | 74.129 | 326.900 | 1.386 | 4.311 |
|  | 2 | 74.019 | 74.019 | 74.019 | 329.250 | 1.396 | 4.337 |
|  | 3 | 74.074 | 74.074 | 74.074 | 329.900 | 1.411 | 4.316 |
|  | 4 | 74.074 | 74.074 | 74.074 | 335.050 | 1.430 | 4.449 |

Figure 32 and Figure 33 show the linear regression line fitted into strain gauge vs piezo film sensor and into accelerometer and piezo film sensor respectively. The frequency of the sieving table does not vary so the plots are perfectly linear.

Figure 32. Frequency linear regression SG vs. PFS

Figure 33. Frequency linear regression accelerometer vs. PFS

Figure 34 and Figure 35 show the linear regression line fitted into amplitude readings of strain gauge and piezo film sensors and accelerometer and piezo film sensors respectively.

Figure 34. Amplitude linear regression SG vs. PFS

Figure 35: Amplitude linear regression accelerometer vs. PFS

Table 5 - Vibration scaling factors

| Type |  | Scaling Factor | R2 |
| --- | --- | --- | --- |
| Frequency | SG vs. PFS | 1 | 1 |
|  | Acc vs. PFS | 1 | 1 |
| Amplitude | SG vs. PFS | 84.806 | 0.9698 |
|  | Acc vs. PFS | 0.3291 | 0.9866 |

Table 5 shows the scaling factors of the vibration regression lines. The correlation coefficient values show that the data is highly correlated and means that the data is linear.

# CONCLUSION AND RECOMMENDATIONS

In conclusion, the purpose of the lab experiment was met, and it resulted that piezo film sensors could replace traditional sensors in dynamic and vibrational measurements with respect to the mining industry. From the transient experiments, it was concluded that piezo film could reliably generate waveform data from transient impacts and that piezo films create a much cleaner and less noisy signal than a strain gauge. The transient experiment concluded in the linearity of the data throughout the whole domain and through peaks. Also, the dynamic response of the data is perfectly linear for the first peak between strain gauge and piezo film sensors. The vibration experiments using the sieving table concluded that piezo film sensors can reliably detect the frequency of the vibrating apparatus to the same degree as strain gauge and accelerometer, produce less noise than a strain gauge sensor especially in lower amplitude vibrations. The linear regression line fitted into frequencies and amplitudes shows the linearity of the data with high correlation coefficients.

There are many applications that these sensors can have an impact on over previously used sensors such as strain gauges and accelerometers in equipment monitoring, rock breaking and blasting. Some primary advantages are that piezo film sensors do not need an input source of power, produce less noise, are more resilient and cheaper than the alternatives. Table 6 describes the positive and negative sides of the use of piezo film sensors.

Table 6 - Positives and negatives of PFS

| Positives | Negatives |
| --- | --- |
| More resilient than strain gauges | High voltage output often requires a voltage divider as they operate up to 100V and most DAQ only gather up to 20V |
| Do not require power source or amplification (little setup to use) | Impractical for non-dynamic environments such as progressive loading (not a universal product like strain gauges) |
| Accuracy in placement not as needed as with strain gauges (or perfect bonding) | Returns a zero-frequency response (although this can be easily filtered) |
| Inexpensive product (~$2) |  |
| Produce less noise than strain gauges |  |

It is recommended to repeat vibration experimentation on the sieving table or any vibrational structure where the frequency of the vibration is adjustable. Also, it is recommended to perform further testing to confirm the reliability of results in different vibrational and transient environments. Possible applications include engines, mills, impact monitoring and VOD analysis. Further testing in velocity of detonation is specifically recommended because there is a potential possibility to improve this analysis’s cost and accuracy. Also, it is recommended to perform further testing with different kinds in size and shape of piezo film sensors to find anomalies.

# References

Measurement Specilaties, Inc. (1999). Piezo Film Sensors Technical Manual. Norristown: Sensor Products Division.

Metra Mess-und Frequenztechnik. (2001). Piezoelectric Accelerometers.

National Instruments. (2016, May 25). Measuring Strain with Strain Gauges. (National Instruments) Retrieved March 30, 2018, from http://www.ni.com/white-paper/3642/en/

National Instruments. (2019, May 24). Measuring Strain with Strain Gauges. (National Instruments) Retrieved March 30, 2018, from http://www.ni.com/white-paper/3642/en/

TE Connectivity. (2019). Piezo Film Sensors. Retrieved March 30, 2018, from http://www.te.com/usa-en/plp/piezo-film-sensors/YG2AA.html

Wong, E. (2015). Split Hopkinson pressure bar. In E. Wong, Robust Design of Microelectronics Assemblies Against Mechanical Shock, Temperature and Moisture (p. 12.2.2).

# APPENDIX

Example of MATLAB code to generate FFT diagram.

% Extract time region of interest from signals

% Generated by MATLAB(R) 9.4 and Signal Processing Toolbox 8.0.

% Generated on: 22-Jul-2019 17:24:36

%%

timeLimits = [43760 45364]; % samples

Channel_1_Data_ROI = Channel_1_Data(:);

Channel_1_Data_ROI = Channel_1_Data_ROI(timeLimits(1):timeLimits(2));

%%

timeLimits = [43760 45364]; % samples

Channel_3_Data_ROI = Channel_3_Data(:);

Channel_3_Data_ROI = Channel_3_Data_ROI(timeLimits(1):timeLimits(2));

%%

timeLimits = [43760 45364]; % samples

Channel_4_Data_ROI = Channel_4_Data(:);

Channel_4_Data_ROI = Channel_4_Data_ROI(timeLimits(1):timeLimits(2));

%%

%Step 2a: Compute the frequency spectrum using FFT

%Variables % Data sampled at 20000 Hz

Fs = 20000;

L=length(Channel_1_Data_ROI);

%FFT Calculations

NFFT= 2^nextpow2(L); % Next power of 2 from length of y

Y= fft(Channel_4_Data_ROI,NFFT)/L; %calculating amplitudes

f= Fs/2*linspace(0,1,NFFT/2+1); %calculating seperate frequencies

%%%%%Step 3a: Plotting next graph in Frequency Domain

figure(1);

plot(f,2*abs(Y(1:NFFT/2 + 1)))

ylabel('Amplitude');

xlabel('Frequency [Hz]');

title('Frequency Domain of Signal Data');

## Piezo film sensor specifications

FEATURES

- Thin piezo film sensor

- Flexible leads give flat profile to the sensor

- Dynamic strain sensing with a high output

- Typical interface to a 1 or 10 M Ω input impedance

- Output Voltage (dependent on force applied)

10 mV to 100V

APPLICATIONS

- Sensing Direct Contact Force

- Recording Time of an Event

- Counting Number of Impact Events

- Measuring Impact Related Events

- Sensing Vibration using Cantilevered Beam

- Wakeup Switch

- Motion Detection

FDT SERIES ELEMENTS WITH LEAD ATTACHMENT

SPECIFICATIONS

- Piezo Film Technology

- Flexible Leads

- High Strain Output

- Film Thickness Options

- Lamination Options

- Solderable Connection Pins

The “F” in FDT Series stands for “‘Flexible Leads”. These are rectangle elements of Piezo film with silver ink screen printed electrodes. Rather than making the lead attachment near the sensor, the Piezo polymer tail extends from the active sensor area as flex circuit material with offset traces. This gives a very flat, flexible lead with a connector at the end.

The FDT elements are available in a variety of different sizes and thicknesses. They are available without a laminate (FDT), with a laminated (0.005” mylar) on one side (FLDT) or with tape release layer adhesive (FDT with adh) in the sensor area.

DIMENSIONS and PART NUMBERS

DIMENSION in INCHES (mm)

Model Number

Part Number

Film

thickness

A

Film

B

Electrode

C

Film

D

Electrode

t

(

μm)

Cap

(

nF)

FDT1-028K

1-1002785-1

28

μm

.620 (16)

.485 (12)

9.25 (235)

1.16 (30)

55

1.37

FDT1-052K

2-1002785-1

52

μm

.620 (16)

.485 (12)

9.25 (235)

1.16 (30)

85

.740

| FLDT1-028K | 1-1002786-1 | 28 μm | .620 (16) | .485 (12) | 9.25 (235) | 1.16 (30) | 205 | 1.37 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| FLDT1-052K | 2-1002786-1 | 52 μm | .620 (16) | .485 (12) | 9.25 (235) | 1.16 (30) | 230 | .740 |
| FDT1-028K w/adh-F | 1001777 | 28 μm | .650 (17) | .485 (12) | 5.51 (140) | 1.18 (30) | 125 | 1.37 |

The connector pins on the FDT sensors can be directly soldered to a PCB with a reasonable level of care. This component cannot withstand high temperatures (>80°C) and therefore soldering of the pins to a PCB must be done quickly. A heat sink clamped to the interface area between the film and the crimps will take the heat away from the film. Pre-tin the pins and then quickly solder them to the board. Do not allow the soldering iron to touch the film and do not use a dwell time of more than 5 seconds on the pins. Low temperature solder can also be used.

## Accelerometer specifications

## Signal conditioner specifications

Charge Amplifier							Type 5010B…

Dual Mode Charge Amplifier with Piezotron® Operating Mode

Versatile, simple to use multi-range, line powered amplifier that converts Kistler sensor signals into proportionally controlled voltage. The dual mode allows for signals from either charge (high impedance) type pressure, force or acceleration sensors or voltage (low impedance) types to be processed.

- High and low impedance sensors

- Dynamic and quasistatic measurements

- Automatic zero adjustments

- RS-232C interface

- Ultra high accuracy and low noise

- Ground isolates I/O connectors

Description

Type 5010B… is a versatile, line-powered, dual mode amplifier for use with high impedance (charge mode) or low impedance (voltage mode) sensors. In the charge mode, the unit converts the input charge signal into a voltage proportional to the measurand. The voltage mode provides sensor source current for powering low impedance sensors.

The dual mode charge amplifier can be used to measure dynamic pressure, force, strain and acceleration from piezoelectric sensors. A long time constant mode permits the user to measure short duration static (quasi-static) events. The scale and sensitivity settings are designed to provide a direct readout in volts per mechanical unit eliminating mathematical manipulations. A rear panel receptacle is provided for remote control of the Reset and Operate modes.

A micro-controller controls all Type 5010B… functions and constantly monitors the unit’s condition. Additionally, it continuously checks for input overload and condition of low impedance sensors. LEDs provide operational status while the LCD provides an indication of error overload, sensitivity, scale, time constant, bias and baud rate when RS-232C is activated.

Each unit is extensively tested using an automatic test and calibration system to ensure the highest possible accuracy and quality. A detailed NIST traceable calibration certificate is furnished with each unit.

Application

The primary use for Type 5010B… charge amplifier is to convert the charge signal from a high impedance piezoelectric force, pressure or acceleration type sensor into a high level output voltage and provide excitation power along with signal processing for voltage mode type sensors. When Type 5010B… is used with a voltage mode sensor, the signal polarity as it passes through the amplifier becomes inverted. The dual mode charge amplifier is considered a laboratory type instrument and should be well protected if used in an industrial environment.

Measurement range; pC; ±10 ... 999000. Scale settings 1,2,3,4,5 sequence; MU/V(1); 0.0002 ... 10000000. Sensor sensitivity; pC/MU; 0.01 ... 9990. mV/MU; 0.01 ... 9990. Specification Unit Type 5010B Input

Technical Data

| Connector charge, voltage |  | BNC neg., ground isolated |
| --- | --- | --- |
| Impedance charge mode | Ω | 70 |
| Impedance voltage mode | Ω | 100k parallel with 1 nF |
| Voltage max. | V | 50 |
| Insulation resistance at input | Ω | 1014 |
| Sensor power voltage mode | mA | 4 (2 ... 18 optional) |

| Frequency response: standard filter, Type 5311 (3dB) | Hz | 180000 |
| --- | --- | --- |
| Accuracy (Long time constant) | % | ≤ ± 0.50 |

Time constant (range dependent)

| Long | sec | 0 … 100000 |
| --- | --- | --- |
| Medium | sec | 1 … 10000 |
| Short | sec | 0.01 … 100 |

Time constant resistor

| Long | Ω | >1014 |
| --- | --- | --- |
| Medium | Ω | 1011 |
| Short | Ω | 109 |

Noise

| Referred to with input shield | pCrms | 0.0036 |
| --- | --- | --- |
| 1 pC/V max. (2) | μVrms | 500 |
| 100 pC/V typical (2) | μVrms | 300 |
| 100000 pC/V typical (2) | μVrms | 200 |
| Drift MOSFET leakage current | pC/s | <±0.03 |
| Zero offset in reset typical | mV | 0.50 |

Output:

| Connector, ground isolated |  | BNC neg. |
| --- | --- | --- |
| Impedance | Ω | 100 |
| Voltage range | V | ±10 |
| Current limit | mA | 5 |
| Display | Type | LCD 16 chars. |

Serial interface (RS-232C)

| Connector |  | 9 pin D-Sub. |
| --- | --- | --- |
| Baud Rates |  | 150 … 9600 |
| Maximum cable length | ft | 65 (2500 pF) |
| Remote control connector |  | DIN 45322 6-pol neg. |
| Temperature range operating | °F | 32 … 122 |
| Temperature range storage | °F | –4 … 158 |
| Humidity non-condensing | % | 10 … 90 |

Power line

| Voltage | VAC | 89 … 135 |
| --- | --- | --- |
| Frequency | Hz | 48 … 62 |
| Power consumption max. | VA | 14 |
| Weight without case | lb | 2.8 |
| Dimensions without case | in | 2.8 x 5.1 x 7.25 |

- MU = mechanical unit (e.g., psi, lb, g, etc)

- Referred to output with input shielded

1 g = 9.80665 m/s2, 1 Inch = 25.4 mm, 1 Gramm = 0.03527 oz, 1 lbf-in = 0.113 Nm

| Accessories Included | Type |
| --- | --- |
| • Power cord | 1508 |
| • Remote reset connector | 1564 |
| • Plug-in filter, 180 kHz | 5311 |
| Optional Accessories | Type |
| • 5 m remote control cable | 1455A5 |
| • Remote control box | 5663 |
| • Rack adaptor for 6 each 5010B… Plug-In low pass filters; see filter options below | 5730 |
| Filter Options-Bandwidth Limiting | Type |
| • 1, 1.5, 2.2, 3.3, 4.7, 6.8, 10, 15, 22, 33, 47 | 5311A(x)kHz |
| • 10, 15, 22, 33, 47, 68, 100, 150, 220, 330, 68, 100, 150, 220, 330, 470, 680 | 5313A(x)Hz |

Low pass, 12 dB/Octave Roll-off x = cut-off frequency (-3db)

Ordering Key

Type 5

Variant

Single channel with RS-232C interface

010B0

Single channel with case and RS-232C interface

010B1

Three channel with case and

RS-232C interface, charge only

5814

| Measure | Connect | Amplify | Output | Analyze |
| --- | --- | --- | --- | --- |
| Type 5010B… | Type 1631C… | Type 50… | Type 1511 |  |
| High impedance | 10-32 pos BNC pos. | Charge amplifier | BNC pos. BNC pos. | not supplied |

Fig. 1: High impedance measuring chain

## Accelerometer calibration certificate