MATERIAL PROPERTIES OF MINERALIZED FOAM AND ITS DENSITY DEPENDENCY – A META-STUDY

ALBRECHT GILKA-BÖTZOW*, MARLON ZIMMER And 
Eduardus A.B. Koenders*

*	Institute of Construction and Building Materials (WIB)

Technische Universität Darmstadt

Franziska-Braun-Straße 3, 64287 Darmstadt, Germany

e-mail: gilka-boetzow@wib.tu-darmstadt.de, web page: www.wib.tu-darmstadt.de

Key words: foam concrete, lightweight mineralized foam, meta-study, systematic review transient foam structure

Abstract. The dependency of mineralized foam towards their material properties, such as compressive strength or thermal conductivity, is widely studied and generally known. However, most of the research conducted on this topic so far has been focusing on a very narrow range of densities. This has led to the fact that the current level of knowledge on the thermo-mechanical performance of this versatile material is very concentrated and, therefore, not providing an overall figure that is covering a wide range of densities. To extend this level of knowledge, a meta-study was conducted at the Institute of Construction and Building Materials of the TU Darmstadt consisting of literature data combined with results taken from own lab tests. Aim of this study was to get a full picture of the interdependencies between various thermo-mechanical parameters of the hardened mineralized foam, while covering a wide range of densities. Final results showed a consistent trend, where literature data and lab test results turned out to be very complimentary

- INTRODUCTION

Due to their great band width of possible densities (100 kg/m³ to 2000 kg/m³), their heat insulation capabilities, and their structural strength, foam concretes and mineralized foams form an attractive material group for structural and insulating use. It enables a wide range of possibilities for using these materials in factory buildings or in in-situ applications [1]. Having said that, this variety of applications and material types creates several practical and scientific questions. Most important ones are on the possibility to produce a robust and very lightweight mineralized foam in a constant quality, how to optimize the heat insulation capacity of mineralized foam without a deterioration of its mechanical characteristics, what is the influence of the solid mater ratio in fresh mineral foam on its transient structure, and how does the consistency and hydration of the binder paste affect the very transient structure of mineral foams? Finding answers to these questions poses quite a challenge which can succeed only by adopting scientific methods. Therefore below, results of a meta-study about material properties of mineralized foam and its density dependency are recapitulated and discussed.

- Material

  - Foam

Foam is gas dispersion in a fluid or solid continuous phase [2, 3]. The ISO 862 defines foam as a sequence of gas cells which are divided by thin fluid films. The confined gas volume is dispersed in a relatively small amount of liquid [5]. Like every system of non-miscible phases, foams aren't thermodynamically stable. The basic components tends toward separation and destabilization. Foam is, therefore, a multiphase system with a limited period of persistence [6, 7]. It is the structure of fluid foams that changes continuously because the surface potential tends to a minimum, by minimizing the interfaces between the phases while releasing the stored energy. Surfactants stabilize the foam structure but the destruction of the foam begins immediately after its formation [8, 9]. There are several processes inside a foam which cause its destruction (fig. 1) [7].

|  | coalescence |
| --- | --- |
|  | disproportioning |
|  | drainage |

Figure 1: Process of foam destruction [6, 10].

As shown above, the structure of foam is significantly determined by the actual fraction of air. Given the fact, the specific weight can be a good criterion for characterizing a foam [11]. For aqueous foams, finding the right density is very often a point of scientific discussions [12–14]. Heavy foams tend to drain but are more flowable [15]. But when using them, more water is brought into the mineral foam with corresponding consequences for the cementitious matrix (fig. 4). Lighter aqueous foams are relatively stiff which becomes more explicit in case of applying an overdosage of foaming agent. This may lead to problems for getting foams with a constant void content [15]. Furthermore, the thin lamellas of a light foam with a low water content provoke a lower robustness of the aqueous foam against suction effects i.e. caused by cement particles [16]. Normal densities of the aqueous foams used for mineral foam production range between 60 kg/m³ and 80 kg/m³ [13, 14].

  - Foam concrete and mineralized foam

Foam concrete means a highly porous cementitious material without coarse aggregates  [19–24]. In contrast to autoclaved aerated concrete, foam concrete hardens due to cement hydration. Besides, the two material types show different characteristics in the hardened state [25]. It's possible to differentiate between the various types of foam concrete using dry density or composition. In addition, the used production technique is formative for their characteristics [26, 27]. The publications analyzed for the proposed Meta-study showed many parallels when referring to the different ranges of densities, and when referring to the fact that these ranges were in most cases between 100 kg/m³ and 500 kg/m³ (cf. fig. 5). On the one hand this can be related to the fact that researches were used to specific compositions or, on the other hand, that when producing foam concrete – even in the lab – it is very hard to meet exactly the specified design density [28]. This shows the need to classify different types of foam concrete [26, 29, 30].

Typically the highest density discussed is about 1800 kg/m³. This density is slightly lower than the 2000 kg/m³, which is the normative limit of lightweight concrete [18]. The foam concretes ranging between 1400 kg/m³ and 1800 kg/m³ are often reinforced and find their use in housing or soil applications, however almost always outside Europe [26, 29–35]. For these particular application, in Europe the more expensive lightweight aggregates concrete is normally used [22, 36]. The densities of the second category of foamed cementitious material range between 800 kg/m³ and the priory mentioned 1400 kg/m³ approximately. It is used for structural applications but mostly as fillers or plugs in the mining or tunneling industry [26, 29, 37–40]. This material can, therefore, also be called ‘foam mortar’. A third category used as a robust filler or insulation material has a density of around 400 kg/m³ to 800 kg/m³. This class can be considered to be part of the mineral (fresh state) or mineralized (hardened state) foams [26, 29, 41–43]. All other types of foams, with densities below a dry density of 400 kg/m³ are called lightweight mineral foams and/or mineralized foams, respectively. These types of foams is a relatively new subject that still requires a deep research effort, and is mostly used as an insulation material (tab. 1) [13, 44, 45].

Table 1: Dry density ranges and proposed categorization for porous cementitious foams with aggregates D < 2 mm.

| dry density range [kg/m³] | category |
| --- | --- |
| 1400 – 1800 | (reinforced) foam concrete |
| 800 – 1400 | foam mortar |
| 400 – 800 | mineralized foam |
| < 400 | lightweight mineralized foam |

- Methods

  - Meta-study

A meta-study or extensive data analysis serves primarily as a way to provide a tendency overview of data gathered from a specific subject. To this end, more than 40 specific studies have been combined and evaluated in order to draw conclusions from a wide range of literature data and own lab results. Present meta-study addresses test results of "foam concrete". Each study-topic was done on a series of tests with various properties that was depending on the density of a particular type of foam concrete. Based on the experimental results the tendency calculations of the meta-study were performed.

  - Foam

The here discussed foamed cementitious materials are based on an aqueous foam principle, which is produced with a foam generator. This device merges the three essential substances, water, air and surfactant, into a fresh foam. The concentration of the foam agent can be changed by adjusting the flow ratio between the in the flowing water and air phases. In an air intrusion device, using compressed air, the gas gets merged in the continuous phase and enclosed by the aqueous foam (cf. fig. 2) [46].

Figure 2: Model representation of a foam generation, forming bubbles into the foam via a perforated plate [46].

A porous membrane follows the air intrusion flow leading to a homogenized pore size distribution of the aqueous foam [6, 15]. Here the pores in the accelerated foamed fluid get divided by the shear forces induced by the obstacles [16].

  - Mineralized foam

All foamed cementitious materials discussed in this context are essentially a mix of aqueous foam and a binder matrix. This technique has the methodical advantages that all components can be individually admeasured and analyzed before mixing. This makes the calculation of the mass flow more transparent, and interdependencies between the used materials can be easily identified and considered. Thus for production a three step procedure is often used. First the binder paste will produced in a specific mixer such as a mortar or slurry mixer, which ensures a homogenous paste due to the high shear forces [47, 48]. Next, the foam will be generated as mentioned before. Finally, both components are mixed together in a classical concrete mixer. In this regard it important to consider that big density differences between foam a binder paste often cause obstructions, which may hinder a fast and efficient mixing (cf. fig. 3). Own research showed that shaft mixers are quite suitable for a successful mixing of these two phases [49, 50].

Figure 3: Schematic representation of the mixing systems used for producing mineral foam. From left to right: single-shaft compulsory mixer, two-wave mixer, bucket mixer.

  - Mix design

For analyzing the different test results of foam concrete it is essential to refer to a unique mix design. Such a method exists for ordinary concrete but it does not exist for foam concrete. The following design method serves as a way to classify the different data received from the evaluated articles of the meta-study.

In order to categorize the importance of the various material characteristics, dry density ρd is defined as the principal design parameter. Independent of the water cement ratio w/c used for the binder paste, it is assumed that it has no significant influence on the dry density. Higher water to cement ratios (> 0.4) will produce pore volumes, which in a first step are relatively small, once comparing with the pore volume produced by foam. For lower water cement ratios, the water needed for a chemical optimum will be counterbalanced by water taken from the aqueous foam. For practical reasons, like measuring consistency and viscosity, water is determined from the total mass of binder and solid additives. On this basis their sum mf can be calculated using formula 1.

| mf = ρd / (1 + w/c) | (1) |
| --- | --- |

It is possible to fill the rest of a virtual cubic meter with aqueous foam VF left by summarizing the individual volumes of the binder paste components Vw and Vf, using the respective material densities (formula 2).

| VF = 1 m³ -Vw - Vf | (2) |
| --- | --- |

As mentioned before, the fresh density ρfr of mineral foam is an important parameter to control the quality during the production process (formula 3).

| ρfr =Σ (mF ,mw ,mf) | (3) |
| --- | --- |

Not considering the water in the aqueous foam mFw, as this is done in many publications, is only acceptable for higher dry densities [51]. The mentioned water amount is directly proportional to the created porosity ϕ of the foam and so indirectly proportional to the density of the mineralized foam (formula 4 and 5).

| mΣw = mFw + mF | (4) |
| --- | --- |
| mΣw = ρF + ϕ · 1 m³ | (5) |

From this, the paste, and thus also the amount of mixing water with a given constant water cement ratio, is indirectly proportional to the porosity. For these reasons, together with the real water cement ratio w/zreal, the amount of water in the aqueous foam φmFw, relative to the total water content, rises disproportionally with declining densities (formula 6 and 7).

| φmFw = mFw / mΣw | (6) |
| --- | --- |
| w/zreal = mΣw / mz | (7) |

Figure 4 shows this deviated relationship. There the real water cement ratio and the share of the water of the aqueous foam is plotted against the design density of the mineralized foam. The given graphs reflect the limiting cases of the water cement ratios 0.4 and 0.6 together with the foam densities of 60 kg/m³ and 80 kg/m³.

Figure 4: Calculated dry density vs real w/c ratio, and the percentage of foam water in the total water content.

- Results

  - Density – compressive strength

Results of the meta-study regarding the relationship between compressive strength and density of foamed concrete and mortar are plotted in figure 5. Based on own experimental results, in figure 6, the same relation for lightweight mineralized foams has been provided. In this figure, the characteristic compressive strength is shown for a foam with a dry density of 180 kg/m³ and has an average value of 0,12 N/mm² (5 %-quantile, 90 % confidence band). The distribution curves on the single values as well as on the broad confidence band could be an indication that different failure types occurred, which could be attributed to the different pore size distributions or pore forms (fig. 6).

Figure 5: Relationship between 28-day compressive strength and density of foamed cementitious material as a result of the meta-study [13, 32, 33, 37, 39, 40, 42, 52–61].

Figure 6: Relationship between compressive strength and dry density of mineralized foam 
(about 100 single values).

  - Density – thermal conductivity

The results of the thermal conductivity showed a nearly linear distribution (fig. 7). Especially for lightweight mineralized foams, results plotted in figure 8 show this observation. The regression function represents the average value of thermal conductivity depending on the dry density. From the Gauss distribution, a characteristic value of 0,059 W/(m · K) for a mineralized foam with a design density of 180 kg/m³ is calculated.

Figure 7: Relationship between thermal conductivity and density of foamed cementitious material as a result of a meta-study [56, 58, 60, 62, 63].

Figure 8: Left: Individual values of thermal conductivity at an average sample temperature of 10 °C as a function of dry density of dried cementitious foams. Right: Normal distribution of the parallel shifted values along the regression function [64].

- Concluding summary

Figure 6 shows a linear relationship between the density and compressive strength for a mineralized foam where densities range between 120 kg/m³ and 260 kg/³. The global dependencies shown in figure 5 are characterized by a decreasing gradient for the lower densities. In figure 7 the distribution of the thermal conductivity of mineralized foam for densities ranging between 200 kg/m³ and 1600 kg/m³ is nearly linear. Single evaluated investigations show, however, always a significant scatter of the distribution towards the lower densities. This can lead to a conclusion that there is a potential for a minimized thermal conductivity once lowering the density of mineralized foam. At the same time also the strength will decrease so there is for every application an optimum of thermal conductivity and mechanical strength (fig. 9). This correlation has been quantified and provided in fig. 9.

Figure 9: Correlation of dependencies compressive strength and thermal conductivity from figure 5 and figure 7.

The relatively large spread in results show that there have to be other factors than the density that influence the mechanical or structural-physical characteristics of foamed cementitious materials. Besides the composition of the continuous phase, it is most probably the pore structure of the hardened foams that plays a dominant role. This pore structure is the result of the transient characteristic of the produced mineral foam. Especially for cementitious foams it is possible to analyze the thermo-dynamic processes that occurs inside the foam, and which causes the quasi-meta-stable (instable) nature of the fluid foams. The cementitious hardening process allows to freeze the actual three dimensional structure of a fluid foam in various states. On this bases, values like compressive strength and thermal conductivity are strongly depending on this and are, therefore, still subject of scientific research.

REFERENCES

[1]	H. Mathes: Monodisperse Schäume: Herstellung und Verwendung als strukturiertes Medium für chemische Zweiphasenreaktionen. Universität Bremen (2004)

[2]	Myers, D.: Surfactant Science and Technology. In: Berichte der Bunsengesellschaft für physikalische Chemie 96 (1992) pp. 1898–1898

[3]	Bikerman, J.J.: Physical surfaces. Elsevier (1970)

[4]	Bikerman, J.: Foams. Springer-Verlag, New York (1973)

[5]	Deutsches Institut für Normung: DIN EN ISO 862:1995-10, Grenzflächenaktive Verbindungen - Begriffe, Beuth Verlag

[6]	Schilbach, J.: Entwicklung und Optimierung eines biotechnologischen Verfahrens zur Herstellung von Proteinschaummitteln. Technische Universität Hamburg-Harburg (2005)

[7]	German, J.: Properties of Stabilizing Components in Foams. In: Chem. Eng. (1990) pp. 62–70

[8]	Tscheuschner, H.-D.: Grundzüge der Lebensmitteltechnik. Behr, Hamburg (1999)

[9]	Reul, H.: Handbuch Bauchemie. Verl. für Chem. Industrie Ziolkowsky, Augsburg (1991)

[10]	Caessens, P.W.J.R.: Enzymatic hydrolysis of ß-casein and ß-lactoglobulin. Foam and emulsion properties of peptides in relation to their molecular structure. Wageningen University (1999)

[11]	Lohaus, L.: Konstruktionsleichtbeton unter Verwendung vorgeschäumter Luftporen. , Hannover (2005)

[12]	Baumert, C., Garrecht, H.: Mineralschaum für Anwendungen in der Fertigteilindustrie. In: BWI - Betonwerk International (2015) pp. 60–66

[13]	Pott, J.U.: Entwicklungsstrategien für zementgebundene Schäume. Universität Hannover (2006)

[14]	Karl, S.: Leichtzuschlag-Schaumbeton als Konstruktionsleichtbeton mit abgeminderter Rohdichte. TU Darmstadt (1979)

[15]	Lohaus, L.: Anwendbarkeit vorgeschäumter Luftporen im Betonbau. Fraunhofer-IRB-Verl., Stuttgart (2000)

[16]	Wilson, A.J.: Foams physics, chemistry and structure. Springer, London (1989)

[17]	Deutsche Bauchemie e.V. hrsg: Herstellung von Luftporenbeton, (2001)

[18]	Deutsches Institut für Normung: DIN EN 206-1:2001-07, Beton Teil 1: Festlegung, Eigenschaften, Herstellung und Konformität, Beuth Verlag

[19]	Weigler, H., Karl, S., Jaegermann, C.: Leichtzuschlag-Beton mit hohem Gehalt an Mörtelporen. In: Deutscher Ausschuss für Stahlbeton 321 (1981)

[20]	Deutsches Institut für Normung: DIN 4164:1951-10, Gas- und Schaumbeton - Herstellung, Verwendung und Prüfung, Richtlinien - zurückgezogen, Beuth Verlag

[21]	Deutsches Institut für Bautechnik: DIBt Mitteilungen Nr. 6:2002-12, Herstellung und Verwendung von Schaumbeton, DIBt

[22]	Deutsches Institut für Normung: DIN EN 206:2014-07, Festlegung, Eigenschaften, Herstellung und Konformität, Beuth Verlag

[23]	Just, A.: Untersuchungen zur Weiterentwicklung von chemisch aufgetriebenen, lufthärtenden, mineralisch gebundenen Schäumen. Universität Dortmund (2008)

[24]	Stegemann, R.: Das grosse Baustoff-Lexikon. Handwörterbuch der gesamten Baustoffkunde. Deutsche Verlags-Anstalt, Stuttgart (1941)

[25]	Grübl, P., Weigler, H., Sieghart, K.: Beton : Arten, Herstellung und Eigenschaften. Ernst, Berlin (2001)

[26]	Ramamurthy, K., Kunhanandan Nambiar, E.K., Indu Siva Ranjani, G.: A classification of studies on properties of foam concrete. In: Cement and Concrete Composites 31 (2009) pp. 388–396

[27]	Nambiar, E.K.K., Ramamurthy, K.: Air-void characterisation of foam concrete. In: Cement and Concrete Research 37 (2007) pp. 221–230

[28]	Stark, J.: Dauerhaftigkeit haufwerksporiger Leichtbetone mit Schaummörtelbindung. Fraunhofer IRB-Verlag, Stuttgart (2003)

[29]	Global Construction: Ultimate Concrete Opportunities (2005 : University of Dundee) creator: Use of foamed concrete in construction proceedings of the international conference held at the University of Dundee, Scotland, UK on 5 July 2005. Thomas Telford, London, UK (2005)

[30]	Dhir, R.K., Henderson, N.A.: Specialist techniques and materials for concrete construction. Thomas Telford (1999)

[31]	Kearsley, E., Booysens, P.: Reinforced Foamed Concrete-Can It Be Durable? In: Concrete Beton (1998)

[32]	Lee, Y., Hung, Y.: Exploitation of Solid Wastes in Foamed Concrete–Challenges Ahead. Proceedings of International Concrete Congress. S. 15–22 (2005)

[33]	Hamidah, M., Azmi, I., Ruslan, M., Kartini, K., Fadhil, N.: Optimisation of foamed concrete mix of different sand–cement ratio and curing conditions. Use of foamed concrete in construction. S. 37–44. , Thomas Telford: London, UK (2005)

[34]	Remadnia, A., Dheilly, R.M., Laidoudi, B., Quéneudec, M.: Use of animal proteins as foaming agent in cementitious concrete composites manufactured with recycled PET aggregates. In: Construction and Building Materials 23 (2009) pp. 3118–3123

[35]	Pedraza, A.R.M., Constantiner, J.L.D.: Mixture Design Optimisation Of Cellular Concrete. In: Specialist Techniques and Materials for Concrete Construction: Proceedings of the International Conference Held at the University of Dundee, Scotland, UK on 8-10 September 1999 (1999) pp. 219

[36]	Deutsches Institut für Normung: DIN EN 1520:2011-06, Vorgefertigte Bauteile aus haufwerksporigem Leichtbeton und mit statisch anrechenbarer oder nicht anrechenbarer Bewehrung, Beuth Verlag

[37]	Kearsley, E., Mostert, H.: Designing mix composition of foamed concrete with high fly ash contents. Use of foamed concrete in construction. London: Thomas Telford. S. 29–36 (2005)

[38]	Jones, M.R., Mc Carthy, A.: Behaviour and assessment of foamed concrete for construction applications. Use of foamed concrete in construction. S. 61–88. Thomas Telford, London, UK (2005)

[39]	Stürmer, S.: Injektionsschaummörtel für die Sanierung historischen Mauerwerks unter besonderer Berücksichtigung bauschädlicher Salze. Bauhaus-Universität Weimar, Weimar (1997)

[40]	Cox, L., van Deijk, S.: Foam concrete. In: Concrete 25 (2002) pp. 54–55

[41]	Cox, L.: Major Road and Bridge Projects with Foam Concrete. Proceedings: International Conference on the Use of Foamed Concrete in Construction, University of Dundee, Scotland, July. S. 105–112 (2005)

[42]	Tikalsky, P.J., Pospisil, J., MacDonald, W.: A method for assessment of the freeze-thaw resistance of preformed foam cellular concrete. In: Cement and Concrete Research 34 (2004) pp. 889–893

[43]	American Concrete Institute: ACI 523.1R:1992, Guide for Cast-in-Place Low Density Cellular Concrete, ACI

[44]	Akthar, F.K., Evans, J.R.G.: High porosity (90%) cementitious foams. In: Cement and Concrete Research 40 (2010) pp. 352–358

[45]	Schneider, J., Garrecht, H., Maier, A., Gilka-Bötzow, A.: Ein multifunktionales und energetisch aktives Fassadenelement aus Beton. In: Bautechnik 91 (2014) pp. 167–174

[46]	Bals, A.: Verfahrenstechnik und Substratfaktoren beim Aufschäumen mit Membranen. VDI-Verl., Düsseldorf (2002)

[47]	MAT Mischanlagentechnik GmbH hrsg: Chargen-Suspensionsmischer Typ SC-05-K

[48]	Baumert, C.: Rheometrische Mischprozessführung Intensiv-Konus-Mischer mit integriertem Rheometer zur Herstellung von Hochleistungsbeton mit definierten rheologischen Eigenschaften. TU Darmstadt, Darmstadt (2012)

[49]	Gilka-Bötzow, A.: Mineralisierter Schaum. In: Beiträge zum 51. DAfStb Forschungskolloquium 2 (2010) pp. 709–720

[50]	Deutsches Institut für Normung: DIN 459-1:1995-11, Baustoffmaschinen Mischer für Beton und Mörtel - Begriffe, Leistungsermittlung, Größen, Beuth Verlag

[51]	Narayanan, N., Ramamurthy, K.: Structure and properties of aerated concrete: a review. In: Cement and Concrete Composites 22 (2000) pp. 321–329

[52]	Hunaiti, Y.M.: Composite Action of Foamed and Lightweight Aggregate Concrete. In: Journal of Materials in Civil Engineering 8 (1996) pp. 111–113

[53]	Kearsley, E.P.: The effect of high volumes of ungraded fly ash on the properties of foamed concrete. University of Leeds, Leeds (1999)

[54]	Kearsley, E.P., Wainwright, P.J.: The effect of high fly ash content on the compressive strength of foamed concrete. In: Cement and Concrete Research 31 (2001) pp. 105–112

[55]	Bucher, A., Yao, Y.: Einfluss von Kunststofffasern auf die Eigenschaften von Schaumbeton. ETH Zürich, Zürich (2006)

[56]	Aldridge, D.: Introduction to foamed concrete: What, why and how? Use of foamed concrete in construction. S. 1–14. Thomas Telford, London, UK (2005)

[57]	Kearsley, E.P., Mostert, H.F.: Opportunities For Expanding The Use Of Foamed Concrete In The Construction Industry. Use of foamed concrete in construction. S. 144–154. , Thomas Telford: London, UK (2005)

[58]	Awang, H., Mydin, M.A.O., Roslan, A.F.: Effect of additives on mechanical and thermal properties of lightweight foamed concrete. In: Pelagia Res. Libr 3 (2012) pp. 3326–3338

[59]	Taylor, R.: Foamed Concrete: Composition and Properties. British Cement Association, Crowthorne (1991)

[60]	Moorfield, G.: Filling a gap in the market. In: Concrete 28 (1994) pp. 12–14

[61]	Kearsley, E.P., Wainwright, P.J.: Ash content for optimum strength of foamed concrete. In: Cement and Concrete Research 32 (2002) pp. 241–246

[62]	Giannakou, A., Jones, M.R.: Potential Of Foamed Concrete To Enhance The Thermal Performance Of Low-Rise Dwellings. Innovations and Developments in Concrete Materials and Construction: Proceedings of the International Conference held at the University of Dundee, Scotland, UK on 9-11 September 2002. S. 533–544. Thomas Telford, London (2002)

[63]	Mydin, A.O.: Effective thermal conductivity of foamcrete of different densities. In: Concrete Research Letters 2 (2011) pp. 181–189

[65]	Gilka-Bötzow, A., Koenders, E.A.B.: Rheological behavior of the continuous phase of foams and its effect on the dispersed phase. In: Proceedings of 24. Workshop und Kolloquium Rheologische Messungen an Baustoffen (2015)

The binder paste influences the foam structure already only due its relatively high density.

Open porous materials don't have a dispersed phase therefore they aren't foams within this definition [4].

Foams with a high gas volume are called colloid agglomerated gas dispersion, otherwise it is by definition no foam but an emulsions of gas [1].

The porosity normally is way higher than in an air-entrained concrete [17].

For this reason actually it is not really correct to define it a concrete. It would be better to speak from foam mortar [18].

In order to calculate this single value for one density all results were moved parallel along the linear regression function.