## Slide 1
REALIZATION OF NEUROMORPHIC SYSTEMS FOR THE DETECTION, TRANSDUCTION AND CLASSIFICATION OF BIO-ELECTRONIC SIGNALS
POLITECNICO DI TORINO
Department of Electronics and Telecommunications Master’s Degree Course in Nanotechnologies for ICTs
Supervisor:
Prof. Matteo COCUZZA
Co-Supervisors:
Dr. Simone Luigi MARASSO
Dr. Silvia BATTISTONI
Prof. Victor EROKHIN
A.Y. 2021/2022
Candidate:
Luciano Ferrucci

## Slide 2: Contents
Luciano Ferrucci
Memristors;
Inkjet printing technologies;
Project goals;
Fabrication process;
Inkjet printing optimization;
Electrical characterization;
Conclusions and future perspectives.

## Slide 3: Memristors
Luciano Ferrucci
They were proposed by Leon Chua in 1971[1].
They show a non-linear behavior, with a memory effect.
Application fields include neuromorphic systems, information and storage processing, communication systems and non-linear circuits.
Memristors can be distinguished according to the materials used for their fabrication, such as resistive, spintronic, ferroelectric and organic memristors.
The four fundamental two-terminal circuit elements [2].
Current-Voltage curve of an ideal memristor [3].

## Slide 4: Organic memristors
Luciano Ferrucci
They can be based on small molecules, conjugated and nonconjugated polymers, biomolecules, nanoparticles.
Polymers like Polyaniline (PANI) show an evident variation of their conductivity according to their redox state, during the redox reaction with the electrolyte.
They were proposed for neuromorphic computing, information and storage processing applications.
They are low-power consuming, reliable, low-cost, with high integration density and biocompatibility.
Additive manufacturing techniques, such as inkjet printing, allow to reduce the production costs and time, increasing the process throughput, without affecting the devices performance.

## Slide 5: Inkjet printing technologies
Luciano Ferrucci
Successful for MEMS, printable electronics, but also for optoelectronics, microfluidics and energy storage applications.
Pros: low cost, low material waste and scaling-up to large industrial production.
Cons: resolution limited to µm sizes. Possible solutions are top-down or bottom-up approaches.
Continuous InkJet (CIJ) and Drop-On-Demand (DOD).
Different actuation principles, in particular a DOD piezoelectric actuation is used in this work.

## Slide 6: Piezoelectric actuation principle
Luciano Ferrucci
Piezoelectric actuation scheme, adapted from [4].
The piezoelectric nozzle is stimulated by a properly defined voltage signal waveform.
The drop ejection is the result of the expansion and contraction of the chamber.
Inkjet printer setting parameters to be properly chosen:
  Rise time and fall time
  Dwell time
  Dwell voltage
  Echo time (i.e. dwell time after the fall time)
  Echo voltage (i.e. dwell voltage after the fall time)
  Back-pressure
  Spot spacing and spot margin
  Fly velocity
Ink drop ejection [5].

## Slide 7: Project goals
Luciano Ferrucci
Fabrication of memristive devices;
Optimization of inkjet printing process, in terms of ink properties and inkjet printer parameters;
Analysis of two ink drying procedures, compared from the morphological standpoint;
Electrical characterization of inkjet-printed organic memristors, comparing the two dry procedure cases.

## Slide 8: Fabrication process
Luciano Ferrucci
Standard cleanroom process steps:
b)
Titanium deposition
c)
Gold deposition
a)
Silicon+Silicon dioxide
substrate
d)
Photoresist spin-coating

## Slide 9: Devices layout optimization
Luciano Ferrucci
The devices layout was optimized on CleWin CAD software, passing from 8 to 16 devices per each die.
3 geometries of interest, distinguished by:
  Channel width fixed to W=[250;500;2000] µm (w250, w500, w2000);
  For each geometry, the channel length is varied L=[10;50;100;200] µm.
w250
Old version
w250
New version
*
W=250 µm
L=200 µm
*
19,92 mm
15,92 mm
27,9 mm
16,1 mm

## Slide 10: Devices layout optimization
Luciano Ferrucci
w2000
Old version
w500
New version
19,92 mm
15,92 mm
27,3 mm
17,2 mm
19,92 mm
15,92 mm
26,4 mm
20 mm
w2000
New version
w500
Old version

## Slide 11: Photolithography
Luciano Ferrucci
e)
LASER writing
f)
Photoresist
development
5 inches UV mask for LASER writing, snapshot taken from CleWin CAD software.
5 inch
16,1 mm
27,9 mm

## Slide 12: Fabrication process
Luciano Ferrucci
g)
Metal wet etching and
photoresist removal
Wafer LASER cutting
h)
i)
Inkjet printing
Final devices, after step (h).

## Slide 13: Inkjet printing optimization
Luciano Ferrucci
Ink synthesis procedure was optimized, reducing the clogging problem due to presence of aggregates in the ink solution.
  PANI 100 kDa powder dissolved in DMSO and the solution was filtered with 22 nm-sized PTFE filters.
Three ink concentrations were tested onto devices with interdigitated channels, whose sizes are LxW=10x9590 µm:
  100 µg/ml;
  250 µg/ml;
  500 µg/ml.

## Slide 14: Ink characterization
Luciano Ferrucci
Inkjet printer parameters for the three ink concentrations
Voltage signal waveforms for the three ink concentrations

## Slide 15: Ink characterization
Luciano Ferrucci
The resistance decreases as the ink concentration increases.
The resistance decreases as the number of printed PANI layers increases.
The best results, in terms of conduction, are the ones with 5 layers at 500 µg/ml.
Field Emission Scanning Electron Microscopy (FESEM) session was executed to investigate the morphology of printed patterns.

## Slide 16: FESEM results – 2 PANI layers @ 500 µg/ml
Luciano Ferrucci

## Slide 17: FESEM results – 5 PANI layers @ 500 µg/ml
Luciano Ferrucci

## Slide 18: Inkjet printer parameters optimization
Luciano Ferrucci
Spot parameters optimization tests. The best results are the ones in the highlighted rows.
Voltage signal waveform parameters used for the printing on the final devices.

## Slide 19: Inkjet printer parameters optimization – poor results
Luciano Ferrucci

## Slide 20: Inkjet printer parameters optimization – best results
Luciano Ferrucci

## Slide 21: Drying procedure
Luciano Ferrucci
Two drying procedures were considered:
  Short and fast dry, by exposing the samples to heat, provided by a hot plate set @80°C;
  Long and slow dry, by leaving the samples at the ambient temperature (i.e. 25°C).
The morphology in these two cases was analyzed and compared, evaluating the printed area on the devices channels.
The short dry strategy provided larger printed area and a not uniform PANI volume, with the presence of lumps due to the fast solvent evaporation.
The long dry strategy, instead, provided less printed area, more repeatable results and a uniform PANI volume on the samples.
Printed area as function of the devices channel aspect ratio. Graph in logarithmic scale.

## Slide 22: Drying procedure – short vs long dry process
Luciano Ferrucci
Short dry
PANI Lumps
Long dry

## Slide 23: Electrical characterization
Luciano Ferrucci
The measurements were executed at CNR-IMEM in Parma.
The instrumentation provides a triangular voltage sweep, swept on the drain contact, while the source one is grounded.
An electrical current in the channel can be measured.
The experimental setup included the use of a liquid electrolyte (HCl) and a third electrode (reference or gate, made of silver) to acquire the ionic current contribution.
PDMS chambers were fabricated and used to host the liquid electrolyte during the acquisitions.
Experimental setup of the electrical characterization tests.
Gate
Drain
Devices
Source

## Slide 24: Hysteresis
Luciano Ferrucci
The differential current is evaluated as the difference between the acquired drain-source current (electronic+ionic) and the gate one (ionic).
As a result, the electronic contribution is extracted.
At PANI oxidation starts (channel switch ON).
Maximum current peak at (high conductance state).
At PANI reduction dominant (channel switch OFF, low conductance state).
Minimum and maximum conductance values and from the hysteresis curves as function of scan rate (i.e. acquisition frequency).
Stable behavior in the most performing devices.
Fast dried devices are more conductive but less repeatable and predictable than slowly-dried ones.

## Slide 25: Hysteresis-Results
Luciano Ferrucci
Example of and vs scan rate,
WxL=250x10 µm short dry device.
vs channel aspect ratio, short and long dry comparison.
Scan rate at 200 mV/s. Main graph in semi logarithmic scale,
inset one in logarithmic scale.

## Slide 26: Kinetics in voltage and time
Luciano Ferrucci
To prove the dependence of the memristance on voltage pulse amplitude (kinetics in voltage) and time width (kinetics in time).
Kinetics in voltage: voltage pulse amplitudes applied for 5 s. Pre and post-writing pulses at for 1 s. Erasing pulse at for 5 s.
Kinetics in time: voltage pulse amplitude fixed to , while the pulses time width values were . Pre and post-writing pulses at for 1 s. Erasing pulse at for 5 s.
The equivalent synaptic weight variation was computed in the two cases, by extracting the conductance values from the pre and post-writing currents.
Kinetics in voltage response WxL=250x10 µm short dry device. Inset graph: input pulses.
Kinetics in time response WxL=250x10 µm short dry device. Inset graph: input pulses.

## Slide 27: Kinetics in voltage-Results
Luciano Ferrucci
a)
b)
c)
d)
w250 long dry devices;
w500 long dry devices;
w2000 long dry devices;
Twin devices, WxL=500x10 µm, short vs long dry case;

## Slide 28: Kinetics in time-Results
Luciano Ferrucci
a)
b)
c)
d)
w250 long dry devices;
w500 long dry devices;
w2000 long dry devices;
Twin devices, WxL=500x10 µm, short vs long dry case;

## Slide 29: Endurance
Luciano Ferrucci
It is the number of writing cycles appliable before breaking down the device.
The ON and OFF current contributions vs the number of writing cycles were extracted.
Stable behavior for 2000 writing cycles at least.
The geometry factor influenced the performances, since devices with high W/L aspect ratio showed better results, in terms of ON/OFF ratio.
Higher ON/OFF ratio=higher classification

## Slide 30
Endurance-Results
WxL=250x10 µm, long dry, ON/OFF;
WxL=2000x10 µm, long dry, ON/OFF ;
WxL=2000x100 µm, short dry, ON/OFF
a)
b)
c)

## Slide 31: LTP & LTD
Luciano Ferrucci
Long-Term Potentiation (LTP) is a synaptic strength enhancement.
  An increasing number of positive voltage pulses results in a higher and higher electrical conduction.
  Pulse amplitude , time width 100 ms.
  Pre and post-writing voltage for 1 s.
  Reset voltage for 5 s.
Long-Term Depression (LTD) is a synaptic strength reduction.
  An increasing number of negative voltage pulses results in a lower and lower electrical conduction.
  Pulse amplitude , time width 100 ms.
  Pre and post-writing voltage for 1 s.
  Reset voltage for 5 s.
In both cases, [1;5;10;30;50;100] pulses are applied.
Good response in all the tested devices.
LTP,
input
pulses
LTD,
input
pulses

## Slide 32: LTP & LTD-Results
Luciano Ferrucci
a)
b)
c)
d)
w250 long dry devices;
w500 long dry devices;
w2000 long dry devices;
Twin devices, WxL=500x10 µm, short vs long dry case;

## Slide 33: Conclusions and future perspectives
Luciano Ferrucci
The devices layout was optimized, increasing the number of samples submitted to the printing procedure.
Inkjet printing process was optimized, in particular:
  ink synthesis, concentration and number of printed layers, guaranteeing appreciable conduction values;
  Inkjet printer settings, from the voltage signal waveform parameters to the spot ones.
Two dry procedures compared from the morphological point of view:
  The fast dry impacts upon the repeatability and reliability of the devices;
  The long dry provides higher repeatability and predictability.
Organic memristors were electrically characterized, comparing the two dry strategies:
  As a consequence of the morphology, fast dried devices performances were more variable and unpredictable;
  Long dried devices, instead, were more reliable and predictable;
  From the functional standpoint, both fast and slowly dried devices showed a feasible response, promising for neuromorphic applications.
Future work perspectives could be a further optimization of the inkjet printing process, by investigating new solvents and improving the inkjet printer parameters. Nevertheless, it would be interesting the implementation of a ANN based on inkjet printed organic memristors.

## Slide 34: References
Luciano Ferrucci
[1] Leon O. Chua. Memristor—the missing circuit element. IEEE Transactions on Circuit Theory, 18:507–519, 1971. doi: 10.1109/TCT.1971.1083337
[2] Georgios Ch. Sirakoulis, Leon O. Chua and Andrew Adamatzky. Handbook Of Memristor Networks. Springer, 2019. doi: 10.1007/978-3-319-76375-0.
[3] Alexandre Yasuo Yamamoto. Memristor engineering: modeling, fabrication and characterization. PhD thesis, Texas AM University, 2019.
[4] Alessio Bucciarelli, Chandrakanth Reddy Chandraiahgari, Andrea Adami, Viviana Mulloni, and Leandro Lorenzelli. Precise dot inkjet printing thought multifactorial statistical optimization of the piezoelectric actuator waveform. Flexible and Printed Electronics, 5, 10 2020. doi: 10.1088/2058-8585/ABBB7E.
[5] http://microfab.com

## Slide 35: Thank you for your attention!
Luciano Ferrucci