## Slide 1
Master Thesis of Marco Giolitti
Surface Passivation Strategies of Perovskite Solar Cells
Reviewers: U. W. Paetzold, F. Bella
Advisor: M. A. Ruiz-Preciado

## Slide 2: Index
Motivation – 3
Perovskite properties – 5
Methods – 7
Treatments – 8
Characterization – 12
Conclusion – 15

## Slide 3: Motivation
NASA, Vital Signs of the Planet, Global Temperature; BP energy charting tool
Climate change
Fossil fuel dependency

## Slide 4: Solar photovoltaics
Office of Scientific and Technical Information, DOE; Bódis et al., 2019, doi: 10.1016/j.rser.2019.109309; National Renewable Energy Laboratory
Huge rooftop potential
Efficiency trend

## Slide 5: Perovskites
3D bulk structure (ABX3)
2D perovskites (R2An-1BnX3n+1)
G. Grancini and M. K. Nazeeruddin, 2019. doi: 10.1038/s41578-018-0065-0.
n=1
n=2
A: Cs+, MA+, FA+
B: Pb2+
X: I-, Br-,Cl-
Composition: Cs0.05MA0.1FA0.85Pb(I0.9Br0.1)3
Phenethylammonium (PEA)

## Slide 6: Surface recombination
Defect-driven recombination
conduction band
valence band
trap state
e-
h+
glass
ITO
2PACz
3D perovskite
C60/BCP
Ag
energy

## Slide 7: Surface modification treatments
glass
ITO
2PACz
3D perovskite
C60/BCP
Ag
2D perovskite
3D perovskite
Cool down
2D perovskite
Single treatment
Dual treatment
PEA salt
IPA
PEA salt + additive
IPA +
DMF
MAI
FAI

## Slide 8: Single treatments
Cs0.05MA0.1FA0.85Pb(I0.9Br0.1)3
PEA salt↑ ⇒ VOC↑
⇒ JSC↓
Reduced current extraction

## Slide 9: Dual treatments
Cs0.05MA0.1FA0.85Pb(I0.9Br0.1)3
Lower JSC deficits
Using MAI or FAI is equal
Different real performance

## Slide 10: Fluorinated dual treatments
Again higher real performance
Cs0.05MA0.1FA0.85Pb(I0.9Br0.1)3
Inferior JSC and FF

## Slide 11: Double cation perovskite
Cs0.12FA0.88PbI3
Similar VOC boost
No drop in JSC and FF

## Slide 12: Photoluminescence quantum yield
Cs0.05MA0.1FA0.85Pb(I0.9Br0.1)3
VOC boost of 30 to 40 mV

## Slide 13: CELIV characterization
Charge extraction with linearly increasing voltage
Cs0.05MA0.1FA0.85Pb(I0.9Br0.1)3

## Slide 14: X-ray diffraction
Cs0.05MA0.1FA0.85Pb(I0.9Br0.1)3
Indications of 2D phases with PEACl treatment
Largely unaffected 3D lattice
: 3D perovskite
peaks

## Slide 15: Conclusion
Composition: Cs0.05MA0.1FA0.85Pb(I0.9Br0.1)3
Optimized PEA-based surface treatments increase VOC by up to 40 mV
Higher JSC for dual treatments
PCE improvement close to 1%abs with PEACl+MAI treatment

## Slide 16: Conclusion
Composition: Cs0.12FA0.88PbI3
Surface treatments boost VOC by 40 mV and do not decrease FF and JSC
PCE improvement of 1%abs with the single PEACl treatment

## Slide 17: Thank you for the attention

## Slide 18: BACK-UP

## Slide 19: Rooftop potential
Most of it is economically favorable
Bódis et al., 2019, doi: 10.1016/j.rser.2019.109309

## Slide 20: Double cation perovskite
Champion device treated with PEACl

## Slide 21: CELIV formulas
Dark-CELIV
  Series resistance:
  Capacitance:
  RC effect correction:
Photo-CELIV
  Mobility:
  Extracted carriers:

## Slide 22: Photoluminescence quantum yield
Implied VOC determination
glass
ITO
2PACz
perovskite
C60/BCP
glass
ITO
2PACz
perovskite

## Slide 23: Surface treatments
Spin coating
2D perovskites
100°C
e-
h+

## Slide 24: Surface modification solutions
Single treatment
Double treatment
PEA salt
IPA
PEA salt + additive
IPA +
DMF
MAI
FAI