## Slide 1
Redesign of 180nm CMOS-MEMS sensors and interface for bioinspired processing
Master's Thesis
Presented by
Leonardo Santoro
Advisor: Daniel Fernández Martínez
Co-advisor: Jordi Madrenas Boadas
Co-advisor: Matteo Cocuzza
Barcelona, September 2023

## Slide 2
Who am I ?
Leonardo Santoro
Date of birth: 20/08/1999 Nationality: Italian
Master's student in Electronic Engineering at the Polytechnic of Turin with a master's degree in CMOS-MEMS focused on the design, migration and characterization of a pressure sensor and an accelerometer. Highly motivated and enthusiastic seeking opportunities to contribute to the development of innovative solutions mainly in the field of healthcare and interested in utilizing my expertise to facilitate advancements in the medical industry. I am dedicated to acquiring new knowledge and skills to better understand the underlying purpose of a project, with the aim of making a meaningful impact for a better society. I strongly believe in the power of teamwork and thrive in a collaborative environment. I find great satisfaction in working with others towards a common goal. I actively contribute to fostering a strong sense of unity within a team, ensuring that every member is supported and no one is left behind. I value open communication, respect diverse perspectives, and strive to create an inclusive and productive work environment.
09/2018 –10/2021
University studies at Sapienza University of Rome-Electronic Engineering
(Bachelor degree)
Email: leonardo.santoro999@gmail.com
Phone: (+39) 3496887650
LinkedIn: https://www.linkedin.com/in/leonardo-santoro-elettronica/
09/2021 – Current
University studies at Politecnico di Torino-Electronic Engineering (master’s degree)
09/2022 – 09/2023
Participation ERASMUS + / PROGRAM COUNTRIES MOBILITY PROGRAM a.y. 2022/2023 courses + thesis in Barcellona, Spain, Universitat Politècnica de Catalunya · Barcelona Tech - UPC, Carrer de Jordi Girona, 31, 08034 Barcelona.
09/2020 – 09/2021
Member of the Sapienza Fast Charge Team for the construction of a vehicle
1

## Slide 3
Contents
Contents
Contents
Contents
Contents
Contents
Contents
Contents
Contents
Contents
Contents
Contents

## Slide 4
Contents
2
General statements on CMOS-MEMS state of the art
Introduction
01
Description on how to implement a migration process to UMC technology in all its part both for pressure sensor and accelerometer design previously made in TSMC
Migration from TSMC to UMC
02
Description on simulations performed in COMSOL on the pressure sensor and the accelerometer; different conditions are discussed for each sensor, distinguishing from their post and pre-fabrication case. The effect of the squeeze film damping that acts on the central resonators is discussed.
COMSOL Simulations
03
A general comparison between the transistors belonging to the two different technologies TSMC and UMC is discussed. An operational amplifier made in TSMC is re-designed (schematic and layout) in UMC using Cadence Tool. Both DRC and LVS of the new design is analysed.
Electronic part: operational amplifier migration
04

## Slide 5
Introduction
CMOS-MEMS state-of-the-art
They have been implemented in a variety of applications, including atmospheric pressure or acceleration sensing. They are expected to continue to be optimized in the future due to the high demand of wearable devices.
MEMS-electronics integration allows to determine the most important specification parameters together with the electronics, thus, allowing the immediate read out of pressure, or more generally of the external physical perturbation
Daniel Fernández , Piotr Michalik, Juan Valle , Saoni Banerji , Josep Maria Sánchez-Chiva , and Jordi Madrenas, IEEE SENSORS JOURNAL, VOL. 23, NO. 2, 15 JANUARY 2023
01
3

## Slide 6
Introduction
CMOS-MEMS state-of-the-art
Resonant Capacitive Pressure sensors: based on the detection of pressure-induced changes in the resonant frequency or on the quality factor of a micro-mechanical structure.
Interdigitated comb Accelerometers: based on the external excitation force that provokes changes of the stress distribution
Spring mass damped systems, described by the Newton’s second law of motion. The systems oscillate at the fundamental frequency, eigenfrequency (or natural frequency)
01
4

## Slide 7
Migration from TSMC to UMC
5
7
6
4
3
2
1
Preparation and Design Analysis
Analysis of the DRM’s
Technology Characterization
Understanding the most important differences between TSMC and UMC process technologies:
Grid size
Layout Migration
manual draw of each layer in shapes according to the design and ensuring adherence to UMC's design rules
Process Compatibility Check
Final validation of the layout against UMC's process design rules and guidelines
Design Verification
Both MEMS system and CMOS circuitry (readout), if present, can be simulated and tested before manufacturing
Layout Verification
Design rule check (DRC) verification. For single MEMS migration no need of layout vs. schematic (LVS) verification
GDSII Generation
The GDSII layout file represents the final layout representation
Fabrication
02
Prototypes-A1 of the Resonant Capacitive Pressure sensor [“Resonant MEMS Pressure Sensor in 180 nm CMOS Technology Obtained by BEOL Isotropic Etching” Diana Mata-Hernandez, Daniel Fernández, Saoni Banerji and Jordi Madrenas] and the Accelerometer layout migration
DRC
5

## Slide 8
Migration from TSMC to UMC
02
Thin Oxide for device and interconnection
P+ S/D implantation
Contact hole between Metal1 and thin oxide
Metal1
Via1 between Metal1 and Metal2
Metal2
Metal3
Metal4
Via4 between Metal4 and Metal5
Metal5
Via5 between Metal5 and Metal6
Metal6
Passivation Pad opening
Pressure sensor Layers
Dummy Layers
DRC
6

## Slide 9
Migration from TSMC to UMC
02
UMC
TSMC
Hierarchy: it allows for a well organization of the design, DRC of single blocks can be performed, single blocks can be re-used.
Expected errors
Springs
° Length of the Vias: the manufacturer imposes a fixed width for the vias.
° Missing slotting metal: it states that the width and the length of a certain metal should be limited. Those errors occurred for the Metal1 and Metal3, that belong to the bottom plate and bottom cavity seal respectively.
Accelerometer
The Metal4 layer that runs along the edges represents the metal in which capacitance sensing is performed by the external circuit.
 | Width central resonator plate
 | Length central resonator plate
 | Perforation length
 | Spacing between perforations
 | Air gap
 | Thickness central plate resonator
 | Mass central plate resonator
 | Quality factor
 | Resonance frequency
 | Damping coefficient
 | Stiffness constant
 | Width central resonator plate
 | Length central resonator plate
 | Perforation length
 | Spacing between perforations
 | Air gap
 | Thickness central plate resonator
 | Mass central plate resonator
 | Quality factor
 | Resonance frequency
 | Damping coefficient
 | Stiffness constant
 | Width central resonator plate
 | Length central resonator plate
 | Perforation length
 | Spacing between perforations
 | Air gap
 | Thickness central plate resonator
 | Width central resonator plate
 | Length central resonator plate
 | Perforation length
 | Spacing between perforations
 | Air gap
 | Thickness central plate resonator
Parameters 180nm TSMC capacitive resonant pressure sensor prototype-A1 pre-fabrication
Parameters 180nm TSMC capacitive resonant pressure sensor prototype-A1 post-fabrication [1]
DRC
7

## Slide 10
COMSOL Simulations
All of the reported simulations are related to the TSMC versions of the sensors.
Easy to change colors, photos and Text.
Easy to change colors, photos and Text.
Easy to change colors, photos and Text.
Easy to change colors, photos and Text.
03
The differences found between the pre and post-fabrication case of the pressure sensor provide a fixed variation introduced This is applied to the accelerometer, which has not been released at the moment
 | Width central resonator plate
 | Length central resonator plate
 | Perforation length
 | Spacing between perforations
 | Air gap
 | Thickness central plate resonator
 | Mass central plate resonator
 | Quality factor
 | Resonance frequency
 | Damping coefficient
 | Stiffness constant
 | Width central resonator plate
 | Length central resonator plate
 | Perforation length
 | Spacing between perforations
 | Air gap
 | Thickness central plate resonator
 | Mass central plate resonator
 | Quality factor
 | Resonance frequency
 | Damping coefficient
 | Stiffness constant
 | Width central resonator plate
 | Length central resonator plate
 | Perforation length
 | Spacing between perforations
 | Air gap
 | Thickness central plate resonator
 | Width central resonator plate
 | Length central resonator plate
 | Perforation length
 | Spacing between perforations
 | Air gap
 | Thickness central plate resonator
Parameters 180nm TSMC capacitive resonant pressure sensor prototype-A1 pre-fabrication
Parameters 180nm TSMC capacitive resonant pressure sensor prototype-A1 post-fabrication [1]
Pressure sensor
8

## Slide 11
COMSOL Simulations
Simulations of sensors represent a pivotal role on a design, allowing to predict the behaviour of the sensor under various conditions depending on several factors such as materials, external stresses, dimensions and geometric composition of the layers used.
All of the reported simulations are related to the TSMC versions of the sensors. Two main designs regarding the pressure sensor have been carried out, these will be referred as the pre-fabricated and the post-fabricated case of study.
Easy to change colors, photos and Text.
Easy to change colors, photos and Text.
Easy to change colors, photos and Text.
Easy to change colors, photos and Text.
03
The differences found between the pre and post-fabrication case of the pressure sensor have made it possible to suppose an ideal, constant variation introduced by the manufacturing process which can also be applied to the accelerometer itself, which has not been released at the moment, in order to suppose its future behaviour.
 | Width central resonator plate
 | Length central resonator plate
 | Perforation length
 | Spacing between perforations
 | Air gap
 | Thickness central plate resonator
 | Mass central plate resonator
 | Quality factor
 | Resonance frequency
 | Damping coefficient
 | Stiffness constant
 | Width central resonator plate
 | Length central resonator plate
 | Perforation length
 | Spacing between perforations
 | Air gap
 | Thickness central plate resonator
 | Mass central plate resonator
 | Quality factor
 | Resonance frequency
 | Damping coefficient
 | Stiffness constant
 | Width central resonator plate
 | Length central resonator plate
 | Perforation length
 | Spacing between perforations
 | Air gap
 | Thickness central plate resonator
 | Width central resonator plate
 | Length central resonator plate
 | Perforation length
 | Spacing between perforations
 | Air gap
 | Thickness central plate resonator
Parameters 180nm TSMC capacitive resonant pressure sensor prototype-A1 pre-fabrication
Parameters 180nm TSMC capacitive resonant pressure sensor prototype-A1 post-fabrication [1]
Pressure sensor: central resonator simplification
9

## Slide 12
COMSOL Simulations
Easy to change colors, photos and Text.
Easy to change colors, photos and Text.
Easy to change colors, photos and Text.
Easy to change colors, photos and Text.
03
Pre-fabrication Pressure sensor: Mechanical characteristics
10

## Slide 13
COMSOL Simulations
Easy to change colors, photos and Text.
Easy to change colors, photos and Text.
Easy to change colors, photos and Text.
Easy to change colors, photos and Text.
03
Post-fabrication Pressure sensor: Mechanical characteristics
Supposed thickness due to manufacturing process (within 20%):
11

## Slide 14
COMSOL Simulations
Easy to change colors, photos and Text.
Easy to change colors, photos and Text.
Easy to change colors, photos and Text.
Easy to change colors, photos and Text.
03
Post-fabrication Pressure sensor: Mechanical characteristics
Supposed thickness due to manufacturing process (within 20%)
Pull-in at around
12
As the theory explain, the pull-in (condition of divergence) arises at 1/3 of the air gap between the two electrodes:

## Slide 15
COMSOL Simulations
Easy to change colors, photos and Text.
Easy to change colors, photos and Text.
Easy to change colors, photos and Text.
Easy to change colors, photos and Text.
03
Post-fabrication Pressure sensor: relative external pressure and bias applied
Pull-in at around
Total displacement of the movable plate and sensed Capacitance of the pressure sensor at 30V of Biasing with respect the variation of the external pressure from 0Pa to 50kPa
13

## Slide 16
COMSOL Simulations
Easy to change colors, photos and Text.
Easy to change colors, photos and Text.
Easy to change colors, photos and Text.
Easy to change colors, photos and Text.
03
Pre-fabrication Accelerometer: mechanical characteristics
Total displacement of the movable plate and sensed Capacitance of the pressure sensor at 30V of Biasing with respect the variation of the external pressure from 0Pa to 50kPa
The central resonator:
14

## Slide 17
COMSOL Simulations
Easy to change colors, photos and Text.
Easy to change colors, photos and Text.
Easy to change colors, photos and Text.
Easy to change colors, photos and Text.
03
Pre-fabrication Accelerometer: sensing capacitance
15

## Slide 18
COMSOL Simulations
Easy to change colors, photos and Text.
Easy to change colors, photos and Text.
Easy to change colors, photos and Text.
Easy to change colors, photos and Text.
03
Post-fabrication Accelerometer
Regarding the vertical sqeeze film damping affecting the central resonating part of this structure, it results much higher with respect the pressure sensor due to the high number of smaller perforations. (damping of with Bao’s model). On the contrary the horizontal relative pressure variation is much smaller smaller.
Sensors differences: | Pressure sensor TSMC |  |  | Accelerometer TSMC |  | 
 | Pre | Post | Correction factor pre-post | Pre | Post | Correction factor pre-post
mass homogeneous (kg) | 1.8995 | 1.7149 | 1.1076 |  | 4.6596 | 1.1076
vertical Resonance frequency (kHz) | 147.16 | 134.69 | 1.093 | 106.89 | 100.52 | 1.063
vertical Stiffness(N/m) | 162.39 | 122.82 | 1.322 | 232.796 | 185.87 | 1.252
Sensors differences: | Pressure sensor TSMC |  |  | Accelerometer TSMC |  | 
 | Pre | Post | Correction factor pre-post | Pre | Post | Correction factor pre-post
 | 1.8995 | 1.7149 | 1.1076 |  | 4.6596 | 1.1076
vertical Resonance frequency (kHz) | 147.16 | 134.69 | 1.093 | 106.89 | 100.52 | 1.063
vertical Stiffness(N/m) | 162.39 | 122.82 | 1.322 | 232.796 | 185.87 | 1.252
Accelerometer |  | Pre-fabrication |  | Post-fabrication
horizontal fr (kHz) |  | 471.46 |  | 477.23
horizontal k (N/m) |  | 4528.889 |  | 4189.516
16

## Slide 19
COMSOL Simulations
Easy to change colors, photos and Text.
Easy to change colors, photos and Text.
Easy to change colors, photos and Text.
Easy to change colors, photos and Text.
Sensors comparisons, correction factors
Regarding the vertical sqeeze film damping affecting the central resonating part of this structure, it results much higher with respect the pressure sensor due to the high number of smaller perforations. (with Bao’s model). On the contrary the vertical relative pressure variation is much smaller smaller.
Sensors differences: | Pressure sensor TSMC |  |  | Accelerometer TSMC |  | 
 | Pre | Post | Correction factor pre-post | Pre | Post | Correction factor pre-post
mass homogeneous (kg) | 1.8995 | 1.7149 | 1.1076 |  | 4.6596 | 1.1076
vertical Resonance frequency (kHz) | 147.16 | 134.69 | 1.093 | 106.89 | 100.52 | 1.063
vertical Stiffness(N/m) | 162.39 | 122.82 | 1.322 | 232.796 | 185.87 | 1.252
Sensors differences: | Pressure sensor TSMC |  |  | Accelerometer TSMC |  | 
 | Pre | Post | Correction factor pre-post | Pre | Post | Correction factor pre-post
 | 1.8995 | 1.7149 | 1.1076 |  | 4.6596 | 1.1076
vertical Resonance frequency (kHz) | 147.16 | 134.69 | 1.093 | 106.89 | 100.52 | 1.063
vertical Stiffness(N/m) | 162.39 | 122.82 | 1.322 | 232.796 | 185.87 | 1.252
Accelerometer | Pre-fabrication | Post-fabrication
horizontal fr (kHz) | 471.46 | 477.23
horizontal k (N/m) | 4528.889 | 4189.516
Pre-fabrication case:
 | Single arm length
 | Spacing between arms
 | Single arm width
 | Horizontal air gap between fixed and movable electrodes
 | Single arm length
 | Spacing between arms
 | Single arm width
 | Horizontal air gap between fixed and movable electrodes
 |  | NEW version(Post-fabrication) |  | old version (Post-Fabrication)
horizontal fr (kHz) |  | ≅53 |  | 477.23
horizontal k (N/m) |  | ≅58 |  | 4189.516
Vertical fr (kHz) |  | ≅26 |  | 134.69
Vertical k (N/m) |  | ≅14 |  | 122.82
Horizontal Q |  | ≅53.8 |  | ≅48
vertical q |  | ≅29 |  | ≅80
03
Post-fabrication case:
17

## Slide 20
COMSOL Simulations
Easy to change colors, photos and Text.
Easy to change colors, photos and Text.
Easy to change colors, photos and Text.
Easy to change colors, photos and Text.
Alternative design Accelerometer
Sensors differences: | Pressure sensor TSMC |  |  | Accelerometer TSMC |  | 
 | Pre | Post | Correction factor pre-post | Pre | Post | Correction factor pre-post
mass homogeneous (kg) | 1.8995 | 1.7149 | 1.1076 |  | 4.6596 | 1.1076
vertical Resonance frequency (kHz) | 147.16 | 134.69 | 1.093 | 106.89 | 100.52 | 1.063
vertical Stiffness(N/m) | 162.39 | 122.82 | 1.322 | 232.796 | 185.87 | 1.252
Sensors differences: | Pressure sensor TSMC |  |  | Accelerometer TSMC |  | 
 | Pre | Post | Correction factor pre-post | Pre | Post | Correction factor pre-post
 | 1.8995 | 1.7149 | 1.1076 |  | 4.6596 | 1.1076
vertical Resonance frequency (kHz) | 147.16 | 134.69 | 1.093 | 106.89 | 100.52 | 1.063
vertical Stiffness(N/m) | 162.39 | 122.82 | 1.322 | 232.796 | 185.87 | 1.252
Accelerometer |  | Pre-fabrication |  | Post-fabrication
horizontal fr (kHz) |  | 471.46 |  | 477.23
horizontal k (N/m) |  | 4528.889 |  | 4189.516
Pre-fabrication case:
Post-fabrication case:
 | Single arm length
 | Spacing between arms
 | Single arm width
 | Horizontal air gap between fixed and movable electrodes
 | Single arm length
 | Spacing between arms
 | Single arm width
 | Horizontal air gap between fixed and movable electrodes
 | NEW version(Post-fabrication) | old version (Post-Fabrication)
horizontal fr (kHz) | ≅53 | 477.23
horizontal k (N/m) | ≅58 | 4189.516
Vertical fr (kHz) | ≅26 | 134.69
Vertical k (N/m) | ≅14 | 122.82
Horizontal Q | ≅53.8 | ≅48
vertical q | ≅29 | ≅80
03
DRC
18

## Slide 21
COMSOL Simulations
Easy to change colors, photos and Text.
Easy to change colors, photos and Text.
Easy to change colors, photos and Text.
Easy to change colors, photos and Text.
03
Alternative design Accelerometer
 | Single arm length
 | Spacing between arms
 | Single arm width
 | Horizontal air gap between fixed and movable electrodes
 | Single arm length
 | Spacing between arms
 | Single arm width
 | Horizontal air gap between fixed and movable electrodes
 |  | NEW version(Post-fabrication) |  | old version (Post-Fabrication)
horizontal fr (kHz) |  | ≅53 |  | 477.23
horizontal k (N/m) |  | ≅58 |  | 4189.516
Vertical fr (kHz) |  | ≅26 |  | 134.69
Vertical k (N/m) |  | ≅14 |  | 122.82
Horizontal Q |  | ≅53.8 |  | ≅48
vertical q |  | ≅29 |  | ≅80
DRC
19

## Slide 22
04
A COMPARISON between the two manufacturers devices has been performed in Cadence between the following transistors:
-nmos2v (TSMC) and N_18_MM (UMC)
-pmos2v (TSMC) and P_18_MM (UMC)
-nmosnvt2v (TSMC) and N_ZERO_18_MM (UMC)
Electronic part: operational amplifier migration
Outputs |  | TSMC |  |  |  | UMC |  | 
 | nmos2v | pmos2v | nmosnvt2v | N_18_MM | N_LV_18_MM | N_ZERO_18_MM | P_18_MM | P_LV_18_MM
length standard at 180nm | 2um | 2um | 2um | 2um | 2um | 2um | 2um | 2um
width standard at 180nm | 10um | 10um | 10um | 10um | 10um | 10um | 10um | 10um
Idrain | 10uA | -10.0014uA | 10uA | 10uA | 10uA | 10uA | -10uA | -10uA
Vgs | 553.822mV | -694.04mV | 152.234mV | 457.1mV | 149.8mV | 34.98mV | -744.7mV | -452.1mV
Vearly | 21.4947V | 30.3472V | 888.713mV | 8.281V | 1.248V | 38.68mV | 40.74mV | 20.1V
Vth | 468.762mV | -479.05mV | 63.3612mV | 348.5mV | 67.76mV | -143.5mV | -481.5mV | -223mV
gm | 125.158uS | 70.551uS | 183.97uS | 135.2uS | 164.6uS | 46.61uS | 67.61uS | 74.85uS
gds | 465.23nS | 329.565uS | 11.2522uS | 1.208uS | 8.016uS | 258.5uS | 245.4nS | 497.4nS
Vov=Vgs-Vth | 85.06mV | -214.99mV | 88.8728mV | 102.6mV | 82.04mV | 178.48mV | -263.2mV | -229.1mV
op. region | 2 | 2 | 2 | 2 | 2 | 1, Vds=Vgs<Vov | 2 | 2
Transistors | Width | Length | Multiplier
MP2, MP3 |  |  | 
MP1, MP0 |  |  | 
MN0, MN1 |  |  | 
MN2 |  |  | 
MN5, MN4 |  |  | 
MN8 |  |  | 
MP4<1:5> |  |  | 
MN10<1:5> |  |  | 
Transistors | Width | Length | Multiplier
MP2, MP3 |  |  | 
MP1, MP0 |  |  | 
MN0, MN1 |  |  | 
MN2 |  |  | 
MN5, MN4 |  |  | 
MN8 |  |  | 
MP4<1:5> |  |  | 
MN10<1:5> |  |  | 
20

## Slide 23
A COMPARISON between the two manufacturers devices has been performed in Cadence between the following transistors:
-nmos2v (TSMC) and N_18_MM (UMC)
-pmos2v (TSMC) and P_18_MM (UMC)
-nmosnvt2v (TSMC) and N_ZERO_18_MM (UMC)
A connection diode like optimized for the n-mos and p-mos respectively to reduce voltage fluctuations and parasitic capacitances
Electronic part: operational amplifier migration
Outputs |  | TSMC |  |  | UMC |  |  | 
 | nmos2v | pmos2v | nmosnvt2v | N_18_MM | N_LV_18_MM | N_ZERO_18_MM | P_18_MM | P_LV_18_MM
length standard at 180nm | 2um | 2um | 2um | 2um | 2um | 2um | 2um | 2um
width standard at 180nm | 10um | 10um | 10um | 10um | 10um | 10um | 10um | 10um
Idrain | 10uA | -10.0014uA | 10uA | 10uA | 10uA | 10uA | -10uA | -10uA
Vgs | 553.822mV | -694.04mV | 152.234mV | 457.1mV | 149.8mV | 34.98mV | -744.7mV | -452.1mV
Vearly | 21.4947V | 30.3472V | 888.713mV | 8.281V | 1.248V | 38.68mV | 40.74mV | 20.1V
Vth | 468.762mV | -479.05mV | 63.3612mV | 348.5mV | 67.76mV | -143.5mV | -481.5mV | -223mV
gm | 125.158uS | 70.551uS | 183.97uS | 135.2uS | 164.6uS | 46.61uS | 67.61uS | 74.85uS
gds | 465.23nS | 329.565uS | 11.2522uS | 1.208uS | 8.016uS | 258.5uS | 245.4nS | 497.4nS
Vov=Vgs-Vth | 85.06mV | -214.99mV | 88.8728mV | 102.6mV | 82.04mV | 178.48mV | -263.2mV | -229.1mV
op. region | 2 | 2 | 2 | 2 | 2 | 1, Vds=Vgs<Vov | 2 | 2
Transistors | Width | Length | Multiplier
MP2, MP3 |  |  | 
MP1, MP0 |  |  | 
MN0, MN1 |  |  | 
MN2 |  |  | 
MN5, MN4 |  |  | 
MN8 |  |  | 
MP4<1:5> |  |  | 
MN10<1:5> |  |  | 
Transistors | Width | Length | Multiplier
MP2, MP3 |  |  | 
MP1, MP0 |  |  | 
MN0, MN1 |  |  | 
MN2 |  |  | 
MN5, MN4 |  |  | 
MN8 |  |  | 
MP4<1:5> |  |  | 
MN10<1:5> |  |  | 
04
Operational amplifier TSMC schematic Cadence view
Width, length and multiplier for UMC operational amplifier version
21

## Slide 24
Electronic part: operational amplifier migration
Transistors | Width | Length | Multiplier
MP2, MP3 |  |  | 
MP1, MP0 |  |  | 
MN0, MN1 |  |  | 
MN2 |  |  | 
MN5, MN4 |  |  | 
MN8 |  |  | 
MP4<1:5> |  |  | 
MN10<1:5> |  |  | 
Transistors | Width | Length | Multiplier
MP2, MP3 |  |  | 
MP1, MP0 |  |  | 
MN0, MN1 |  |  | 
MN2 |  |  | 
MN5, MN4 |  |  | 
MN8 |  |  | 
MP4<1:5> |  |  | 
MN10<1:5> |  |  | 
04
Operational amplifier TSMC schematic Cadence view
Width, length and multiplier for UMC operational amplifier version
22

## Slide 25
Electronic part: operational amplifier migration
04
23

## Slide 26
Electronic part: operational amplifier migration
04
24

## Slide 27
Electronic part: operational amplifier migration
04
DRC
LVS
25

## Slide 28
Conclusions
04
DRC
LVS
26
Migration from the TSMC to the UMC technology of the prototypes-A1 of a pressure sensor and an accelerometer: the simplicity of migrating an existing design in one technology to another, while maintaining the same technological node, has been demonstrated.
Characterization of the pressure sensor and the accelerometer have been obtained using COMSOL 5.5 tool: some ideal and constant correction factors have been extrapolated in order to be applied to the the accelerometer. Designs' robustness and reliability (stresses) has been checked
Simulations results have been validated against expected performance metrics and experimental results
A new design version of the accelerometer has been proposed with the aim to enhance the sensitivity of it.
Direct comparison between the primary transistors belonging to the TSMC and UMC.
An TSMC operational amplifier has been migrated in UMC technology from scratch: the DRC and LVS procedure using the Cadence tool.

## Slide 29
Conclusions

## Slide 31
THANK YOU FOR YOUR ATTENTION
Presented by LEONARDO SANTORO