## Slide 1
POLITECNICO DI TORINO
MASTER OF SCIENCE IN PETROLEUM AND MINING ENGINEERING
Geomechanical characteristics and karst of gypsum formations at Moncalvo quarry
Candidate Academic Supervisor
Umer Muhammad Prof. Claudio Oggeri
S272626 Academic Co-Supervisor(s)
Prof. Fiorucci Adriano
Academic year: 2023/2024

## Slide 2: Contents
Gypsum Essential Mineral powering Industry, Chemicals and Construction
Gypsum Formation and Regional Ore body types in Geology
Geotechnical Challenges of Gypsum
Karst Hydrogeological Problems
Exploring Quarry Environments, Investigations and Surveys
Quarrying Methods, Techniques for Efficient Extraction
Lab-Based Material Characterization: Data Compilation, Sampling, Testing and Failure Analysis
Observations/Monitoring
Conclusion: Suggestions for Hydro and Geomechanical Monitoring

## Slide 3: Gypsum Essential Mineral powering Industry, Chemicals and Construction
Gypsum, an evaporitic mineral, holds significant importance in various fields.
Gypsum deposits offer insights into past environments and geological processes, aiding in structural geology studies with their layered formations.
Gypsum's properties enable its versatile use in civil engineering for soil stabilization, foundation construction, and as a crucial component in cement and plaster production.
Gypsum, prized for its fire-resistant and soundproofing attributes, is a ubiquitous building material in drywall, plasterboard, and ceiling tile construction globally.
Gypsum's industrial versatility extends to agriculture, medicine, and art due to its roles as a soil conditioner, calcium supplement, and carving material when hydrated.
Gypsum serves as a proppant in hydraulic fracturing, crucial for maintaining fractures in rock formations during oil and gas extraction.

## Slide 4: Gypsum Formation and Regional Ore body types in Geology
Gypsum quarried underground in Monferrato by Fassa Bortolo S.p.A. from the Formazione Gessoso Solfifera, also known as the Complesso Caotico della Valle Versa.
The gypsum deposit being exploited features 10 to 15-meter thick massive macro- and microcrystalline beds separated by marly interstrata of varying thickness.
In Moncalvo, the karst system is categorized as nearby and/or deeply seated due to incomplete dissection of gypsum formations by the surface drainage system.
Gypsum dissolution, notably in upper evaporite beds, is observed in underground mines where drifts carve out small karst cavities.
Rare fractures along over 12 km of drifts in the Moncalvo underground quarry occasionally transport minuscule amounts of water.
The underwater quarry exhibits phreatic morphologies with a uniform roof surface, sporadic cupolas, resembling megascallops, ceiling pendants, and corrosion bevels, devoid of speleothems.
Reference:(Conference paper January 2009, Messinian karst in Monferrato gypsum areas (North Italy) [8].

## Slide 5: Geotechnical Challenges of Gypsum
Mitigating geotechnical challenges in gypsum-rich environments demands meticulous site investigation, precise engineering design, and effective implementation of mitigation measures for structural stability and durability.
Gypsum's solubility in water poses instability risks for structures in gypsum-rich areas, particularly with high groundwater levels or heavy rainfall, as it can dissolve over time when exposed to moisture.
Surface-exposed gypsum is prone to erosion by water, fostering land instability, slope failures, and geomorphological hazards.
Gypsum's reactivity with surrounding minerals or chemicals alters its properties, potentially forming expansive compounds like ettringite, causing soil or rock swelling and cracking.
Gypsum's sensitivity to temperature, such as during freeze-thaw cycles, heightens its propensity for volume changes, posing heightened risks in cold climate regions.
Gypsum deposits may trigger geological hazards like sinkholes or subsidence, particularly in areas with prolonged gypsum dissolution, endangering infrastructure and human safety.

## Slide 6: Karst Hydrogeological Problems
Karst landscapes' rapid water movement via fissures, sinkholes, and conduits heightens vulnerability to contamination from surface pollutants like agricultural runoff, industrial waste, and sewage.
Dissolution of soluble bedrock in karst areas forms sinkholes, posing hazards to infrastructure like roads, buildings, and pipelines.
Karst aquifers display intricate and unpredictable flow patterns due to interconnected conduits and fractures, challenging sustainable groundwater management.
Karst ecosystems are highly sensitive to water quantity and quality changes, impacting biodiversity, habitat stability, and ecosystem services.
Climate change worsens karst hydrogeological issues by altering precipitation, increasing extreme weather events, and amplifying human impacts on water resources.
Subsidence from underground cavity collapse endangers infrastructure and disrupts natural landscapes.
Reference: (Article in Zeitschrift für Geomorphologie Supplementary Issues · May 2010, Hypo gene gypsum karst and sinkhole formation at Moncalvo (Asti, Italy).

## Slide 7: Exploring Quarry Environments, Investigations and Surveys
Karst tunnel behind mining face eroded by decreasing water level; discovered three linked conduits and sizable room
Boreholes equipped with piezometers and automatic rain gauge for monitoring groundwater table in relation to rainfall and mine water pumping.
(GSI) method developed for precise rock mass characterization in engineering rock mechanics; essential for numerical analysis and design of tunnels, slopes, or foundations requiring raw rock property data.
Numerical tools require precise input data on tensile and deformation properties of surrounding rock bulk for tunnel design.
GSI integrates primary geological constraints, including blockiness and discontinuity conditions, serving as a reliable and user-friendly field indicator.
Reference:( Article in Estonian Journal of Earth Sciences · September 2008) [34].

## Slide 8: Quarrying Methods, Techniques for Efficient Extraction
Open-pit mining: Exposing gypsum deposits by removing overburden; Quarrying: Extracting gypsum with drills, explosives, and heavy machinery from near-surface deposits.
Room and pillar mining: Grid-pattern excavation with pillars for support; Long wall mining: Continuous face extraction for efficient gypsum recovery.
Drilling: Precision drilling for blast hole placement; Blasting: Controlled detonation to fragment gypsum for extraction ease.
Reclamation planning: Restoring quarried areas post-extraction; Water management: Mitigating groundwater contamination; Dust control: Minimizing airborne particles with suppression techniques.
Automation: Underground exploitation adopts both blasting techniques and also mechanized excavation by means of road header equipment.
Training programs: Educating workers on safety and best practices; Personal protective equipment (PPE): Ensuring appropriate gear for tasks; Emergency response plans: Establishing procedures for quarry incidents.
Reference: (Article in Zeitschrift für Geomorphologie Supplementary Issues · May 2010, Hypogene gypsum karst and sinkhole formation at Moncalvo (Asti, Italy).

## Slide 9: Collected Specimens

## Slide 10: Lab-Based Material Characterization: Data Compilation
Six gypsum samples were collected from Moncalvo Mining site, comprising three fine-grained and three coarse-grained specimens.
We started specimen preparation with blocks, seeding their prismatic surfaces.
Ensuring material safety results in achieving high strength levels.
Conducted uniaxial compression tests on gypsum samples, followed by microstructural analysis to elucidate deformation and failure mechanisms.
Testing was conducted using Catman Easy by HBM acquisition system on Galdabani equipment with 100-ton load cell, employing two LDVT transducers (HBM, 50mm range, 0.01mm precision) for specimen settlement measurement.

## Slide 11: Fine Grained Specimens (01)

## Slide 12: Fine Grained Specimen (02)

## Slide 13: Fine Grained Specimen (03)

## Slide 14: Sample Testing and Failure Analysis (Fine Grained Specimens)
Specimens before and after Testing
Fine Grained Specimens
Gypsum features a layered structure with calcium ions sandwiched between sulfate tetrahedral sheets.
Our experimental investigation aims to quantify stresses, strains, and Modulus of Elasticity of all specimens.
When stress is applied perpendicular to the mineral's cleavage plane, it exhibits significant plastic deformation and bending, even at high strain rates.
Microstructural analysis of deformed gypsum samples was conducted to understand deformation and failure mechanisms.

## Slide 15: Coarse Grained Specimens (01)

## Slide 16: Coarse Grained Specimen (02)

## Slide 17: Coarse Grained Specimen (03)

## Slide 18: Sample Testing and Failure Analysis (Coarse Grained Specimens)
Specimens before and after Testing
Coarse Grained Specimens
On average, specimens characterized by finer grains tend to exhibit greater strength compared to those characterized by coarser grains.
Each specimen displays peak strength followed by a decrease in residual strength, evidenced by prolonged deformation after failure.
We hypothesize that stress or strain is equivalent to the modulus of elasticity.
Strength is influenced by grain size distribution and statistical factors, the latter being twice as significant.

## Slide 19: Observations/Monitoring
Results obtained of all specimens in the Politechnico di Torino Laboratory.
The test results reveal unexpectedly high strength in the specimens.
Specimen | Mass (g) | Volume cm3 | Mass Volume kg/m3 | UCS MPA | Static Modulus MPa | Pundit time us@250kHz/54kHz | Pundit Velocity m/s | Dynamic Modulus MPa
FG1 | 5571 | 2546 | 2187 | 25.75 | 1840 | 50 | 3820 | 23000
FG2 | 4861 | 2183 | 2226 | 30.70 | 2420 | 50 | 4040 | 25681
FG3 | 6652 | 2995 | 2220 | 23.50 | 1880 | 46 | 4500 | 27992
CG1 | 5884 | 2683 | 2193 | 24.40 | 1740 | 65-50 | 2923/3800 | 15292
CG2 | 6982 | 3025 | 2308 | 21.63 | 1560 | 52 | 3654/4050 | 19181
CG3 | 5129 | 2276 | 2252 | 26.66 | 1840 | 36 | 4944 | 28135

## Slide 20: Conclusion: Suggestions for Hydro and Geomechanical Monitoring
Moncalvo quarry reaches depths of 60 meters below the current thalweg levels, submerged in the deep groundwater flow system with water pressure reaching up to 3 bars.
Mining tunnels intersecting water-filled gypsum caves resulted in a forceful surge of water into passages, subsequently drained; exploration continues until encountering a barrier of silty-clay sediments nearly filling the space.
Geological, structural, and hydrogeological investigations, supported by hydrological monitoring and geophysical surveys, ensure effective risk management and land planning.
Geomechanical behavior of gypsum deposit and marly levels is determined through laboratory testing and in situ monitoring of under ground and ground surface.
To mitigate environmental impact and ensure safe gypsum extraction, conservation of water resources and assessment of karst hazards are crucial considerations.
Anticipating procedures for local geostructural survey, geomechanical characterization, and stope monitoring ensures safe design primarily focused on deformation.

## Slide 21
POLITECNICO DI TORINO
MASTER OF SCIENCE IN PETROLEUM AND MINING ENGINEERING
Thank you for the attention!
Academic year: 2023/2024
Candidate
Umer Muhammad
S272626
Academic Supervisor(s)
Prof. Claudio Oggeri
Academic Co-Supervisor(s)
Prof. Fiorucci Adriano