# Abstract

The building sector accounts for a substantial share of global energy demand and greenhouse gas emissions, with space conditioning dominating operational loads. In Iran—a nation spanning five Köppen-Geiger climate zones—designing energy-efficient envelopes that simultaneously ensure occupant comfort remains a formidable challenge. This thesis introduces a reproducible, simulation-based multi-objective optimization (MOO) framework for the climate-responsive integration of Phase Change Materials (PCMs) in office buildings.

The workflow couples EnergyPlus with the bespoke ChameleonPCM plugin (seamlessly embedded in Rhino/Grasshopper via Honeybee/Ladybug) and the NSGA-II genetic algorithm. Four decision variables—PCM type, melting temperature, layer thickness, and envelope placement—are optimized to minimize annual Energy Use Intensity (EUI) while maximizing Thermal Comfort Percentage (TCP), defined per ASHRAE Standard 55 adaptive criteria. Five cities serve as climatic proxies: Yazd (BWh, hot-desert), Kerman (BWk, cold-desert), Mashhad (BSk, cold semi-arid), Rasht (Cfa, humid subtropical), and Bushehr (BSh, hot-humid).

Pareto frontiers reveal stark climatic dependence. In arid and semi-arid zones exhibiting diurnal swings exceeding 15 °C, optimized PCMs reduce EUI by 9–31 % and sustain or enhance comfort. Peak-performing solutions feature paraffin-based PCMs with melting points of 25–27 °C, 40–50 mm thicknesses, and mid- or interior-side placements that guarantee complete nightly solidification. In humid coastal cities, where swings fall below 7 °C and latent loads prevail, passive PCMs yield negligible gains (<1.5 % EUI reduction) due to incomplete phase-transition cycles.

Future-climate resilience is assessed under RCP 8.5 (2080 horizon). Arid-region benefits persist despite a 4–5 °C ambient rise, whereas humid-zone performance degrades further, underscoring the need for hybrid strategies—e.g., PCMs paired with nocturnal ventilation or desiccant-assisted cooling.

The open-source ChameleonPCM tool and accompanying MOO template empower designers to generate locale-specific guidelines within hours. By quantifying trade-offs and delimiting applicability boundaries, this work bridges the gap between material science and climate-adaptive architecture, furnishing actionable pathways toward net-zero-ready buildings across Iran’s diverse thermal regimes.

Keywords: Phase Change Materials (PCMs), Climate-Responsive Building Design, Energy Efficiency, Thermal Comfort, Simulation-Based Optimization.