Ni foam cs

| Label: | Map Sum Spectrum |
| --- | --- |
| Source: | Acquired |
| Created: | 2025-02-13 2:41:15 PM |
| Livetime: | 144.2s |
| Process Time: | 6 |
| Accelerating Voltage: | 15.00kV |
| Magnification: | 50 x |
| Working Distance: | 10.0mm |
| Specimen Tilt (degrees): | 0.0 |
| Elevation (degrees): | 35.0 |
| Azimuth (degrees): | 0.0 |
| Number Of Channels: | 1024 |
| Energy Range (keV): | 20 keV |
| Energy per Channel (eV): | 20.0eV |
| Detector Type Id: | 26 |
| Detector Type: | X-Act |
| Window Type: | SATW |
| Pulse Pile Up Correction: | Succeeded |

| Element | Wt% | Wt% Sigma | Atomic % |
| --- | --- | --- | --- |
| O | 28.08 | 0.45 | 60.26 |
| Cl | 1.68 | 0.08 | 1.63 |
| Fe | 29.63 | 0.51 | 18.21 |
| Co | 3.36 | 0.30 | 1.96 |
| Ni | 22.38 | 0.49 | 13.09 |
| Cu | 4.10 | 0.98 | 2.22 |
| Zn | 1.61 | 0.40 | 0.85 |
| Mo | 1.07 | 0.30 | 0.38 |
| Au | 8.10 | 0.41 | 1.41 |
| Total: | 100.00 |  | 100.00 |

Ni foam cs

| Label: | Map Sum Spectrum |
| --- | --- |
| Source: | Acquired |
| Created: | 2025-02-13 2:49:31 PM |
| Livetime: | 98.7s |
| Process Time: | 6 |
| Accelerating Voltage: | 15.00kV |
| Magnification: | 50 x |
| Working Distance: | 10.0mm |
| Specimen Tilt (degrees): | 0.0 |
| Elevation (degrees): | 35.0 |
| Azimuth (degrees): | 0.0 |
| Number Of Channels: | 1024 |
| Energy Range (keV): | 20 keV |
| Energy per Channel (eV): | 20.0eV |
| Detector Type Id: | 26 |
| Detector Type: | X-Act |
| Window Type: | SATW |
| Pulse Pile Up Correction: | Succeeded |

| Element | Wt% | Wt% Sigma | Atomic % |
| --- | --- | --- | --- |
| O | 28.83 | 0.36 | 59.05 |
| S | 0.30 | 0.08 | 0.31 |
| Cl | 1.55 | 0.09 | 1.43 |
| Fe | 38.64 | 0.46 | 22.68 |
| Co | 3.68 | 0.35 | 2.05 |
| Ni | 25.49 | 0.49 | 14.23 |
| Au | 1.50 | 0.31 | 0.25 |
| Total: | 100.00 |  | 100.00 |

Ni felt cs

| Label: | Map Sum Spectrum |
| --- | --- |
| Source: | Acquired |
| Created: | 2025-02-13 2:55:11 PM |
| Livetime: | 115.8s |
| Process Time: | 6 |
| Accelerating Voltage: | 15.00kV |
| Magnification: | 30 x |
| Working Distance: | 10.0mm |
| Specimen Tilt (degrees): | 0.0 |
| Elevation (degrees): | 35.0 |
| Azimuth (degrees): | 0.0 |
| Number Of Channels: | 1024 |
| Energy Range (keV): | 20 keV |
| Energy per Channel (eV): | 20.0eV |
| Detector Type Id: | 26 |
| Detector Type: | X-Act |
| Window Type: | SATW |
| Pulse Pile Up Correction: | Succeeded |

| Element | Wt% | Wt% Sigma | Atomic % |
| --- | --- | --- | --- |
| C | 7.79 | 0.42 | 25.76 |
| O | 7.09 | 0.19 | 17.60 |
| Cl | 1.02 | 0.07 | 1.14 |
| Fe | 2.88 | 0.17 | 2.05 |
| Co | 2.33 | 0.24 | 1.57 |
| Ni | 75.71 | 0.53 | 51.23 |
| Au | 3.19 | 0.28 | 0.64 |
| Total: | 100.00 |  | 100.00 |

Ni foam

| Label: | Map Sum Spectrum |
| --- | --- |
| Source: | Acquired |
| Created: | 2025-02-13 3:00:48 PM |
| Livetime: | 125.8s |
| Process Time: | 6 |
| Accelerating Voltage: | 15.00kV |
| Magnification: | 50 x |
| Working Distance: | 17.0mm |
| Specimen Tilt (degrees): | 0.0 |
| Elevation (degrees): | 35.0 |
| Azimuth (degrees): | 0.0 |
| Number Of Channels: | 1024 |
| Energy Range (keV): | 20 keV |
| Energy per Channel (eV): | 20.0eV |
| Detector Type Id: | 26 |
| Detector Type: | X-Act |
| Window Type: | SATW |
| Pulse Pile Up Correction: | Succeeded |

| Element | Wt% | Wt% Sigma | Atomic % |
| --- | --- | --- | --- |
| O | 39.63 | 0.40 | 69.64 |
| S | 0.29 | 0.07 | 0.25 |
| Cl | 1.07 | 0.08 | 0.85 |
| Fe | 40.78 | 0.42 | 20.53 |
| Co | 3.64 | 0.33 | 1.74 |
| Ni | 14.60 | 0.41 | 6.99 |
| Total: | 100.00 |  | 100.00 |

Ni felt

| Label: | Map Sum Spectrum |
| --- | --- |
| Source: | Acquired |
| Created: | 2025-02-13 3:06:40 PM |
| Livetime: | 94.4s |
| Process Time: | 6 |
| Accelerating Voltage: | 15.00kV |
| Magnification: | 50 x |
| Working Distance: | 17.0mm |
| Specimen Tilt (degrees): | 0.0 |
| Elevation (degrees): | 35.0 |
| Azimuth (degrees): | 0.0 |
| Number Of Channels: | 1024 |
| Energy Range (keV): | 20 keV |
| Energy per Channel (eV): | 20.0eV |
| Detector Type Id: | 26 |
| Detector Type: | X-Act |
| Window Type: | SATW |
| Pulse Pile Up Correction: | Succeeded |

| Element | Wt% | Wt% Sigma | Atomic % |
| --- | --- | --- | --- |
| O | 41.30 | 0.34 | 70.83 |
| Si | 0.21 | 0.05 | 0.21 |
| S | 0.67 | 0.07 | 0.57 |
| Cl | 1.35 | 0.07 | 1.05 |
| Fe | 40.07 | 0.36 | 19.69 |
| Co | 4.80 | 0.28 | 2.24 |
| Ni | 11.59 | 0.33 | 5.42 |
| Total: | 100.00 |  | 100.00 |